##### DRAFT EAST AFRICAN STANDARD

Cold formed structural steel sections — Specification

EAST AFRICAN COMMUNITY

Copyright notice

This EAC document is copyright-protected by EAC. While the reproduction of this document by participants in the EAC standards development process is permitted without prior permission from EAC, neither this document nor any extract from it may be reproduced, stored or transmitted in any form for any other purpose without prior written permission from EAC.

Requests for permission to reproduce this document for the purpose of selling it should be addressed as shown below or to EAC’s member body in the country of the requester:

© East African Community 2023 — All rights reserved

East African Community

P.O. Box 1096,

Arusha

Tanzania

Tel: + 255 27 2162100

Fax: + 255 27 2162190

E-mail: eac@eachq.org

Web: www.eac-quality.net

Reproduction for sales purposes may be subject to royalty payments or a licensing agreement. Violators may be prosecuted.

Contents	Page

Foreword	iv

1	Scope	5

2	Normative references	5

3	Terms and definitions	5

4	Symbols	6

5	Dimensions and tolerances	6

5.1	Dimensions	6

5.2	Tolerances	6

5.3	Measurement	7

5.3.1	General	7

5.3.2	Outside dimension	7

5.3.3	Thickness	7

5.3.4	Out-of-roundness	8

5.3.5	Concavity and convexity	8

5.3.6	Squareness	9

5.3.7	External corner profile	9

5.3.8	Twist	10

5.3.9	Straightness	11

6	Compound sections	12

7	Material requirement	12

7.1	Grade designation	12

7.2	Chemical composition	12

7.3	Mechanical properties	12

8	Sampling	13

8.1	General	13

8.2	Test pieces	13

9	Marking	14

Annex A (normative)  Section properties	15

Foreword

Development of the East African Standards has been necessitated by the need for harmonizing requirements governing quality of products and services in the East African Community. It is envisaged that through harmonized standardization, trade barriers that are encountered when goods and services are exchanged within the Community will be removed.

The Community has established an East African Standards Committee (EASC) mandated to develop and issue East African Standards (EAS). The Committee is composed of representatives of the National Standards Bodies in Partner States, together with the representatives from the public and private sector organizations in the community.

East African Standards are developed through Technical Committees that are representative of key stakeholders including government, academia, consumer groups, private sector and other interested parties. Draft East African Standards are circulated to stakeholders through the National Standards Bodies in the Partner States. The comments received are discussed and incorporated before finalization of standards, in accordance with the Principles and procedures for development of East African Standards.

East African Standards are subject to review, to keep pace with technological advances. Users of the East African Standards are therefore expected to ensure that they always have the latest versions of the standards they are implementing.

The committee responsible for this document is Technical Committee EASC/TC 035, Steel and steel products.

This fourth edition cancels and replaces the third edition (EAS 134: 2019), which has been technically revised.

Attention is drawn to the possibility that some of the elements of this document may be subject of patent rights. EAC shall not be held responsible for identifying any or all such patent rights.

Cold formed structural steel sections — Specification

# 1	Scope

This Final Draft East African Standard specifies the requirements and sectional properties of cold formed structural steel sections of thickness of 1 mm to 8 mm for use in structural and general engineering applications.

The sections and their sectional properties are listed in Annex A.

# 2	Normative references

The following document is referred to in the text in such a way that some or all of its content constitutes requirements of this document. For dated references, only the edition cited applies. For undated references, the latest edition of the referenced document (including any amendments) applies.

ISO 148-1, Metallic materials — Charpy pendulum impact test — Part 1: Test method

ISO 404, Steel and steel products — General technical delivery requirements

ISO 1461, Hot dip galvanized coatings on fabricated iron and steel articles — Specifications and test methods

ISO 6892-1, Metallic materials — Tensile testing — Part 1: Method of test at room temperature

ISO 8492, Metallic materials — Tube — Flattening test

ISO 8493, Metallic materials — Tube — Drift-expanding test

ISO 10799-2, Cold-formed welded structural hollow sections of non-alloy and fine grain steels — Part 2: Dimensions and sectional properties

ISO 12633-2, Hot-finished structural hollow sections of non-alloy and fine grain steels — Part 2: Dimensions and sectional properties

ISO 12944-5, Paints and varnishes — Corrosion protection of steel structures by protective paint systemsPart 5: Protective paint systems

ISO 14347, Fatigue — Design procedure for welded hollow-section joints — Recommendations

ISO 16172, Steel sheet, metallic-coated by the continuous hot-dip process for corrugated steel pipe

# 3	Terms and definitions

No terms and definitions are listed in this document.

ISO and IEC maintain terminological databases for use in standardization at the following addresses:

—	ISO Online browsing platform: available at http://www.iso.org/obp

—	IEC Electropedia: available at https://www.electropedia.org

# 4	Symbols

The following nomenclature shall be used. Units for dimensions are in millimetres and those for section properties in centimetres.

- t			section thickness									mm

- p		distance from edge to section centre of gravity	-	cm

- A		sectional area								-	cm2

- Z		section modulus of section l/p					-	cm3

- I			second moment of area						-	cm4

- r			radius of gyration of section lA				-	cm

- x, y		with reference to x or y axis

- w		mass per linear metre							-	kg/m

- L		length										-	m

# 5	Dimensions and tolerances

## 5.1	Dimensions

Dimensions of sections shall be in accordance with those listed in the relevant tables in Annex A.

## 5.2	Tolerances

Tolerances of characteristic properties shall be as given in Table 1.

Table 1 — Tolerances for characteristic properties

| Characteristic | Tolerance |
| --- | --- |
| Outside dimensiona | ±1.5 mm or 2 %, whichever is less |
| Deviation from straightness | 0.17 % of total length |
| Squareness of corners | 90° ± 2° |
| Twist | Not to exceed 2 mm ± 0.5 mm per metre |
| Concavity/convexity | Max. 0.8 %, with a minimum of 0.5 mm for square and rectangular hollow sections |
| Outside bend radii for right angle bends | - If thickness is less than 6 mm, tolerance is between 1.5 t to 2.5 t - If thickness is between 6 mm to 8 mm, tolerance is between 2 t to 3 t |
| Length (6 m): - Exact - Standard | 0 and + 10 mm 0 mm and + 50 mm |
| Thickness | - ±3 % for 1 mm - above 1 mm ± 7.5 % |
| Mass per metre for 1 mm thick | ± 3 % |
| Mass per metre for above 1 mm thick | ± 6.0 % |
| Deviation from out of roundness | - For D/T ratio ≤ 100: ± 2 % - For D/T ratio > 100: ± 2 % by agreement |
| a This tolerance shall be measured at a distance of not less than 100 mm from the end of the section. |  |

## 5.3	Measurement

### 5.3.1	General

All external dimensions including out-of-roundness shall be measured at a distance from the end of the hollow section of not less than D for circular sections, B for square sections or H for rectangular sections, with a minimum of 100 mm.

### 5.3.2	Outside dimension

When inspecting circular hollow sections, the diameter D shall be measured directly. The limiting cross-sectional positions for measuring B and H are shown in Figure 1, and shall be in accordance with Annex A.

### 5.3.3	Thickness

The thickness t shall be measured at a positon not less than 2 t from the weld. The limiting cross-sectional positions for measuring the thickness of square and rectangular sections are shown in Figure 1.

NOTE	Thickness is normally measured within a distance of half of the outside diameter or half of the length of the longer side from the end of the section.

a	This dimension is a maximum when measuring B or H and a minimum when measuring t.

Figure 1 — Limiting cross-sectional positions for measuring the dimensions B, H and t for square or rectangular sections

### 5.3.4	Out-of-roundness

The out-of-roundness, O, of a circular hollow section shall be calculated as follows:

where

D			is the nominal outside diameter of a circular hollow section;

Dmax			is the maximum outside diameter; and

Dmin			is the minimum outside diameter.

### 5.3.5	Concavity and convexity

The concavity (C1) and convexity (C2) of the sides of the square or rectangular hollow section shall be measured as shown in Figure 2.

The percentage concavity C1 shall be calculated as follows:

or

The percentage convexity C2 shall be calculated as follows:

or

where

B and H are the lengths of the sides containing the concavity C1 or convexity C2.

Figure 2 — Measurement of concavity/convexity of square or rectangular hollow sections

### 5.3.6	Squareness

Squareness of the sides of a square or rectangular hollow section shall be measured as difference between 90º and ɵ as shown in Figure 3.

.

Figure 3 — Squareness of sides of square or rectangular hollow sections

### 5.3.7	External corner profile

5.3.7.1	The external corner profile of a square or rectangular hollow section shall be measured in accordance with 5.3.7.2 or 5.3.7.3.

5.3.7.2	The corner arc shall be measured with a radius gauge.

5.3.7.3	The distance between the intersection of the flat side and the corner arc and the intersection of the projections of the flat sides to the corner (C1) and (C2) in Figure 4 shall be measured.

Figure 4 — Outside corner profile of square or rectangular hollow sections

### 5.3.8	Twist

5.3.8.1	The twist (V) in a square or rectangular hollow section shall be determined in accordance with 5.3.8.2 or 5.3.8.3.

5.3.8.2	The hollow section shall be placed on a horizontal surface with one side at one end pressed against the surface. At the opposite end of the hollow section, the difference in height of the two lower corners from a horizontal surface as shown in Figure 5, shall be measured.

Figure 5 — Twist of square or rectangular hollow sections

5.3.8.3	The twist shall be measured with a spirit level and micrometre gauge (screw). The reference length of the spirit level shall be the distance between the intersection of the flat sides and the corner arcs (see Figure 6). The twist V is the difference between the values V1 (see Figure 6) measured at each end of the section.

Figure 6 — Measurement of twist

### 5.3.9	Straightness

The deviation from straightness (e) of total length of a hollow section shall be measured at the point of maximum departure of the hollow section from a straight line connecting its two ends as shown in Figure 7.

The percentage deviation from straightness shall be calculated as follows:

Figure 7 — Measurement of deviation from straightness

# 6	Compound sections

6.1	Compound sections may be formed by suitably connecting two or more simple sections. For example, an 'I' section can be made from two channels back-to-back, a tube from two inwardly lipped channels lip-to-lip, a 'T" from two angles, etc. Methods of joining sections are specified in ISO 14347.

6.2	Section properties of compound sections may be calculated using the properties of simple sections.

6.3	Compound sections shall be flush at matching joints within 2.0 mm.

# 7	Material requirement

## 7.1	Grade designation

The designation of the grades of material shall be based on minimum permissible yield stress and shall be in accordance with Table 2.

Table 2 — Grade designation

| Minimum yield stress N/mm2 | Designation of grade |
| --- | --- |
| 210 | 210 |
| 250 | 250 |
| 360 | 360 |

## 7.2	Chemical composition

The results of ladle chemical analysis of steel from which a hollow section is manufactured shall comply with appropriate limits of Table 3. For grade 360, it shall be permissible to add suitable grain-refining elements to achieve the minimum specified tensile stress, but the total content of these elements shall not exceed 0.15 %.

Table 3 — Ladle chemical analysis limits

| Grade of steel | Maximum content % |  |  |  |
| --- | --- | --- | --- | --- |
|  | Carbon | Phosphorous | Sulphur | Manganese |
| 210 | 0.20 | 0.05 | 0.05 | - |
| 250 | 0.25 | 0.06 | 0.06 | - |
| 360 | - | - | 0.04 | - |

## 7.3	Mechanical properties

The mechanical properties obtained from test samples taken from the hollow section in accordance with ISO 6892-1, shall comply with the requirements given in Table 4. If other grades of steel are used, their mechanical properties shall be as agreed upon between the purchaser and the manufacturer.

Table 4 — Tensile test requirements

| Grade of steel | Minimum yield stress N/mm2 | Ultimate tensile strength N/mm2 | Minimum elongation as a proportion of gauge length % |
| --- | --- | --- | --- |
| 210 | 210 | 340 | 24 |
| 250 | 250 | 420 | 22 |
| 360 | 360 | 480 | 20 |

7.4 Coating properties (If applicable)

The cold formed steel sections may be supplied with or without coatings. When sections are supplied with coatings, sections shall be hot dip galvanized, aluminium zinc coated, pre -painted or in combination.

When sections are hot dip galvanized they shall comply with ISO 1461.

When sections are aluminium zinc coated they shall comply with ISO 16172.

When sections are pre -painted they shall comply with ISO 12944 -5.

# 8	Test methods and sampling

## 8.1	Test methods

8.1.1 Tensile tests

Tensile test to be done according to ISO 6892-1.

8.1.2 Impact tests

Where requested, impact test to be done according to ISO 148-1 and shall be assessed in accordance with ISO 404.

8.1.3 Flattening tests

Flattening test to be done according to ISO 8492 and shall show no sign of cracking.

8.1.4 Flare tests (Drift-expanding tests)

Test to be done according to ISO 8493 and shall not crack or show any other defect.

## 8.2	Sampling

8.2.1	At least one sample shall be selected from the following batch sizes:

- a 20-tonne or less batch of sections having outside diameter of less than 90 mm; and

- a batch of less than 40 tonnes for all other sections.

8.2.2	If the test fails, two more samples shall be drawn from the batch and tested. If one or both test specimens re-tested fail, the whole batch shall be deemed not to have complied with this standard unless all sections in the batch are tested individually.

# 9	Marking

Each piece shall be indelibly and legibly marked at least once in every 6-m length with the following:

- manufacturer’s name and/or registered trademark;

- outside dimension in millimetres;

- nominal thickness in millimetres;

- steel grade; and

- country of origin.

Annex A
(normative)

Section properties

Figure A.1 — Square hollow sections

Table A.1 — Dimensions and properties for cold formed square hollow sections

| Size, B x D mm | Thickness, t mm | Cross-sectional area, A cm2 | Mass, w kg/m | Second moment of area, Ix = Iy cm4 | Radius of gyration, Rx = Ry cm | Section elastic modulus, Zx = Zy cm3 |
| --- | --- | --- | --- | --- | --- | --- |
| 10 x 10 | 1.2 | 0.39 | 0.30 | 0.047129 | 0.349722 | 0.09 |
| 10 x 10 | 1.5 | 0.45 | 0.35 | 0.050548 | 0.334382 | 0.10 |
| 12 x 12 | 1.0 | 0.41 | 0.33 | 0.080793 | 0.441622 | 0.13 |
| 12 x 12 | 1.2 | 0.48 | 0.38 | 0.089707 | 0.431708 | 0.15 |
| 12 x 12 | 1.5 | 0.57 | 0.45 | 0.099303 | 0.416629 | 0.17 |
| 14 x 14 | 1.0 | 0.49 | 0.39 | 0.135455 | 0.523503 | 0.19 |
| 14 x 14 | 1.2 | 0.58 | 0.45 | 0.152281 | 0.513581 | 0.22 |
| 14 x 14 | 1.5 | 0.69 | 0.54 | 0.172098 | 0.498665 | 0.25 |
| 16 x 16 | 1.0 | 0.57 | 0.45 | 0.210312 | 0.605170 | 0.26 |
| 16 x 16 | 1.2 | 0.67 | 0.53 | 0.238689 | 0.595389 | 0.30 |
| 16 x 16 | 1.5 | 0.81 | 0.64 | 0.273736 | 0.580584 | 0.34 |
| 16 x 16 | 2.0 | 1.02 | 0.80 | 0.313845 | 0.555506 | 0.39 |
| 18 x 18 | 1.2 | 0.77 | 0.60 | 0.352772 | 0.677157 | 0.39 |
| 18 x 18 | 1.5 | 0.93 | 0.73 | 0.409015 | 0.662433 | 0.45 |
| 18 x 18 | 2.0 | 1.18 | 0.92 | 0.478445 | 0.637559 | 0.53 |
| 20 x 20 | 1.0 | 0.73 | 0.58 | 0.433771 | 0.768609 | 0.43 |
| 20 x 20 | 1.2 | 0.87 | 0.68 | 0.498369 | 0.758898 | 0.50 |
| 20 x 20 | 1.5 | 1.05 | 0.83 | 0.582737 | 0.744236 | 0.58 |
| 20 x 20 | 2.0 | 1.34 | 1.05 | 0.692186 | 0.719514 | 0.69 |
| 25 x 25 | 1.0 | 0.93 | 0.73 | 0.884200 | 0.972840 | 0.71 |
| 25 x 25 | 1.2 | 1.11 | 0.87 | 1.025440 | 0.963182 | 0.82 |
| 25 x 25 | 1.5 | 1.35 | 1.06 | 1.216722 | 0.948623 | 0.97 |
| 25 x 25 | 2.0 | 1.74 | 1.36 | 1.483530 | 0.924152 | 1.19 |
| 25 x 25 | 2.5 | 2.09 | 1.64 | 1.689908 | 0.899393 | 1.35 |
| 25 x 25 | 3.0 | 2.41 | 1.89 | 1.840962 | 0.874306 | 1.47 |
| 30 x 30 | 1.0 | 1.13 | 0.89 | 1.571411 | 1.177033 | 1.05 |
| 30 x 30 | 1.2 | 1.35 | 1.06 | 1.833477 | 1.167408 | 1.22 |
| 30 x 30 | 1.5 | 1.65 | 1.30 | 2.195967 | 1.152914 | 1.46 |
| 30 x 30 | 2.0 | 2.14 | 1.68 | 2.722004 | 1.128595 | 1.81 |
| 30 x 30 | 2.5 | 2.59 | 2.03 | 3.155984 | 1.104055 | 2.10 |
| 30 x 30 | 3.0 | 3.01 | 2.36 | 3.504194 | 1.079271 | 2.34 |
| 40 x 40 | 1.0 | 1.53 | 1.20 | 3.856181 | 1.585365 | 1.93 |
| 40 x 40 | 1.2 | 1.83 | 1.43 | 4.532452 | 1.575779 | 2.27 |
| 40 x 40 | 1.5 | 2.25 | 1.77 | 5.490241 | 1.561361 | 2.75 |
| 40 x 40 | 2.0 | 2.94 | 2.31 | 6.940341 | 1.537218 | 3.47 |
| 40 x 40 | 2.5 | 3.59 | 2.82 | 8.215307 | 1.512926 | 4.11 |
| 40 x 40 | 3.0 | 4.21 | 3.30 | 9.323785 | 1.488472 | 4.66 |
| 40 x 40 | 4.0 | 5.35 | 4.20 | 11.074982 | 1.439028 | 5.54 |
| 50 x 50 | 1.2 | 2.31 | 1.81 | 9.075294 | 1.984099 | 3.63 |
| 50 x 50 | 1.5 | 2.85 | 2.24 | 11.065556 | 1.969724 | 4.43 |
| 50 x 50 | 2.0 | 3.74 | 2.93 | 14.147198 | 1.945680 | 5.66 |
| 50 x 50 | 2.5 | 4.59 | 3.60 | 16.944192 | 1.921523 | 6.78 |
| 50 x 50 | 3.0 | 5.41 | 4.25 | 19.467546 | 1.897246 | 7.79 |
| 50 x 50 | 4.0 | 6.95 | 5.45 | 23.736481 | 1.848303 | 9.49 |
| 60 x 60 | 1.5 | 3.45 | 2.71 | 19.521915 | 2.378047 | 6.51 |
| 60 x 60 | 2.0 | 4.54 | 3.56 | 25.142576 | 2.354066 | 8.38 |
| 60 x 60 | 2.5 | 5.59 | 4.39 | 30.342640 | 2.329994 | 10.11 |
| 60 x 60 | 3.0 | 6.61 | 5.19 | 35.135477 | 2.305827 | 11.71 |
| 60 x 60 | 4.0 | 8.55 | 6.71 | 43.552060 | 2.257190 | 14.52 |
| 75 x 75 | 2.5 | 7.09 | 5.56 | 61.383242 | 2.942582 | 16.37 |
| 75 x 75 | 3.0 | 8.41 | 6.60 | 71.620192 | 2.918520 | 19.10 |
| 75 x 75 | 4.0 | 10.95 | 8.59 | 90.189328 | 2.870166 | 24.05 |
| 75 x 75 | 5.0 | 13.36 | 10.48 | 106.328271 | 2.821487 | 28.35 |
| 75 x 75 | 6.0 | 15.63 | 12.27 | 120.165935 | 2.772455 | 32.04 |
| 100 x 100 | 3.0 | 11.41 | 8.96 | 177.048901 | 3.939448 | 35.41 |
| 100 x 100 | 4.0 | 14.95 | 11.73 | 226.355174 | 3.891359 | 45.27 |
| 100 x 100 | 5.0 | 18.36 | 14.41 | 271.107073 | 3.843045 | 54.22 |
| 100 x 100 | 6.0 | 21.63 | 16.98 | 311.480730 | 3.794492 | 62.30 |
| 100 x 100 | 8.0 | 27.79 | 21.82 | 379.783697 | 3.696607 | 75.96 |
| 120 x 120 | 3.0 | 13.81 | 10.84 | 312.350633 | 4.756094 | 52.06 |
| 120 x 120 | 4.0 | 18.15 | 14.25 | 402.281212 | 4.708131 | 67.05 |
| 120 x 120 | 5.0 | 22.36 | 17.55 | 485.482240 | 4.659988 | 80.91 |
| 120 x 120 | 6.0 | 26.43 | 20.75 | 562.167626 | 4.611654 | 93.69 |
| 125 x 125 | 3.0 | 14.41 | 11.31 | 354.503672 | 4.960248 | 56.72 |
| 125 x 125 | 4.0 | 18.95 | 14.87 | 457.234021 | 4.912310 | 73.16 |
| 125 x 125 | 5.0 | 23.36 | 18.33 | 552.624938 | 4.864199 | 88.42 |
| 125 x 125 | 6.0 | 27.63 | 21.69 | 640.899775 | 4.815908 | 102.54 |
| 125 x 125 | 8.0 | 35.79 | 28.10 | 775.342601 | 4.654253 | 124.05 |
| 150 x 150 | 4.0 | 22.95 | 18.01 | 807.825868 | 5.933145 | 107.71 |
| 150 x 150 | 5.0 | 28.36 | 22.26 | 982.131865 | 5.885164 | 130.95 |
| 150 x 150 | 6.0 | 33.63 | 26.40 | 1 145.923070 | 5.837039 | 152.79 |
| 150 x 150 | 8.0 | 43.24 | 33.95 | 1 411.866334 | 5.714180 | 188.25 |
| 175 x 175 | 4.0 | 26.95 | 21.15 | 1 303.130714 | 6.953916 | 148.93 |
| 175 x 175 | 5.0 | 33.36 | 26.18 | 1 590.877854 | 6.906026 | 181.81 |
| 175 x 175 | 6.0 | 39.63 | 31.11 | 1 864.050615 | 6.858015 | 213.03 |
| 175 x 175 | 8.0 | 51.79 | 40.66 | 2 325.526067 | 6.700799 | 265.77 |
| 200 x 200 | 4.0 | 30.95 | 24.29 | 1 968.148561 | 7.974648 | 196.81 |
| 200 x 200 | 5.0 | 38.36 | 30.11 | 2 410.112906 | 7.926824 | 241.01 |
| 200 x 200 | 6.0 | 45.63 | 35.82 | 2 832.782410 | 7.878896 | 283.28 |
| 200 x 200 | 8.0 | 59.24 | 46.51 | 3 566.321801 | 7.758946 | 356.63 |
| 250 x 250 | 4.0 | 38.95 | 30.57 | 3 907.323254 | 10.016043 | 312.59 |
| 250 x 250 | 5.0 | 48.36 | 37.96 | 4 805.050198 | 9.968310 | 384.40 |
| 250 x 250 | 6.0 | 57.63 | 45.24 | 5 672.058750 | 9.920496 | 453.76 |
| 250 x 250 | 8.0 | 75.24 | 59.06 | 7 229.321267 | 9.802218 | 578.35 |
| Note: Other dimensions and their sectional properties may be produced according to ISO 10799-2 or ISO 12633-2. |  |  |  |  |  |  |

Figure A.2 ― Rectangular hollow section

Table A.2 – Dimensions and properties for cold formed rectangular hollow sections

| Size, B x D mm | Thickness, t mm | Area, A cm2 | Mass, w kg/m | Second Moment of area |  | Radius of gyration |  | Elastic section modulus |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Major axis x-x Ix cm4 | Minor axis y-y Iy cm4 | Major axis x-x Rx cm | Minor axis y-y Ry cm | Major axis x-x Zx cm3 | Minor axis y-y Zy cm3 |
| 30 x 10 | 1.0 | 0.73 | 0.57 | 0.730 | 0.125 | 1.000 | 0.413 | 0.487 | 0.249 |
| 30 x 10 | 1.2 | 0.87 | 0.68 | 0.838 | 0.141 | 0.984 | 0.403 | 0.558 | 0.281 |
| 30 x 10 | 1.5 | 1.05 | 0.83 | 0.976 | 0.160 | 0.963 | 0.390 | 0.651 | 0.320 |
| 30 x 20 | 1.0 | 0.93 | 0.73 | 1.151 | 0.614 | 1.110 | 0.811 | 0.767 | 0.614 |
| 30 x 20 | 1.2 | 1.11 | 0.87 | 1.336 | 0.711 | 1.099 | 0.802 | 0.890 | 0.711 |
| 30 x 20 | 1.5 | 1.35 | 1.06 | 1.586 | 0.840 | 1.083 | 0.788 | 1.057 | 0.840 |
| 30 x 20 | 2.0 | 1.74 | 1.36 | 1.937 | 1.018 | 1.056 | 0.765 | 1.291 | 1.018 |
| 35 x 15 | 1.0 | 0.93 | 0.73 | 1.39 | 0.37 | 1.22 | 0.63 | 0.79 | 0.49 |
| 35 x 15 | 1.2 | 1.11 | 0.87 | 1.611 | 0.421 | 1.207 | 0.617 | 0.921 | 0.562 |
| 35 x 15 | 1.5 | 1.35 | 1.06 | 1.911 | 0.494 | 1.189 | 0.604 | 1.092 | 0.658 |
| 35 x 15 | 2.0 | 1.74 | 1.36 | 2.327 | 0.589 | 1.157 | 0.582 | 1.330 | 0.785 |
| 35 x 15 | 3.0 | 2.41 | 1.89 | 2.867 | 0.699 | 1.091 | 0.539 | 1.639 | 0.932 |
| 35 x 25 | 1.0 | 1.13 | 0.89 | 1.967 | 1.172 | 1.317 | 1.017 | 1.124 | 0.938 |
| 35 x 25 | 1.2 | 1.35 | 1.06 | 2.297 | 1.366 | 1.307 | 1.008 | 1.312 | 1.092 |
| 35 x 25 | 1.5 | 1.65 | 1.30 | 2.753 | 1.631 | 1.291 | 0.994 | 1.573 | 1.305 |
| 35 x 25 | 2.0 | 2.14 | 1.68 | 3.417 | 2.014 | 1.265 | 0.971 | 1.953 | 1.611 |
| 35 x 25 | 3.0 | 3.01 | 2.36 | 4.408 | 2.571 | 1.210 | 0.925 | 2.519 | 2.057 |
| 35 x 30 | 1.0 | 1.23 | 0.97 | 2.26 | 1.78 | 1.35 | 1.20 | 1.29 | 1.19 |
| 35 x 30 | 1.2 | 1.47 | 1.15 | 2.640 | 2.082 | 1.342 | 1.192 | 1.508 | 1.388 |
| 35 x 30 | 1.5 | 1.80 | 1.41 | 3.174 | 2.501 | 1.327 | 1.178 | 1.814 | 1.667 |
| 35 x 30 | 2.0 | 2.34 | 1.83 | 3.962 | 3.115 | 1.302 | 1.154 | 2.264 | 2.076 |
| 35 x 30 | 3.0 | 3.31 | 2.60 | 5.178 | 4.053 | 1.251 | 1.107 | 2.959 | 2.702 |
| 40 x 10 | 1.0 | 0.93 | 0.73 | 1.574 | 0.165 | 1.298 | 0.421 | 0.787 | 0.331 |
| 40 x 10 | 1.2 | 1.11 | 0.87 | 1.822 | 0.187 | 1.284 | 0.412 | 0.911 | 0.375 |
| 40 x 10 | 1.5 | 1.35 | 1.06 | 2.153 | 0.215 | 1.262 | 0.399 | 1.077 | 0.430 |
| 40 x 10 | 2.0 | 1.74 | 1.36 | 2.604 | 0.247 | 1.224 | 0.377 | 1.302 | 0.494 |
| 40 x 20 | 1.0 | 1.13 | 0.89 | 2.335 | 0.795 | 1.435 | 0.837 | 1.167 | 0.795 |
| 40 x 20 | 1.2 | 1.35 | 1.06 | 2.725 | 0.923 | 1.423 | 0.828 | 1.363 | 0.923 |
| 40 x 20 | 1.5 | 1.65 | 1.30 | 3.266 | 1.097 | 1.406 | 0.815 | 1.633 | 1.097 |
| 40 x 20 | 2.0 | 2.14 | 1.68 | 4.050 | 1.343 | 1.377 | 0.793 | 2.025 | 1.343 |
| 40 x 20 | 3.0 | 3.01 | 2.36 | 5.208 | 1.685 | 1.316 | 0.748 | 2.604 | 1.685 |
| 40 x 25 | 1.0 | 1.23 | 0.97 | 2.715 | 1.316 | 1.483 | 1.033 | 1.358 | 1.053 |
| 40 x 25 | 1.2 | 1.47 | 1.15 | 3.177 | 1.536 | 1.472 | 1.024 | 1.589 | 1.229 |
| 40 x 25 | 1.5 | 1.80 | 1.41 | 3.822 | 1.839 | 1.456 | 1.010 | 1.911 | 1.471 |
| 40 x 25 | 2.0 | 2.34 | 1.83 | 4.772 | 2.279 | 1.429 | 0.988 | 2.386 | 1.823 |
| 40 x 25 | 3.0 | 3.31 | 2.60 | 6.237 | 2.937 | 1.373 | 0.942 | 3.118 | 2.349 |
| 40 x 35 | 1.2 | 1.71 | 1.34 | 4.081 | 3.325 | 1.547 | 1.396 | 2.040 | 1.900 |
| 40 x 35 | 1.5 | 2.10 | 1.65 | 4.934 | 4.017 | 1.532 | 1.382 | 2.467 | 2.295 |
| 40 x 35 | 2.0 | 2.74 | 2.15 | 6.218 | 5.053 | 1.507 | 1.359 | 3.109 | 2.887 |
| 40 x 35 | 3.0 | 3.91 | 3.07 | 8.295 | 6.719 | 1.457 | 1.311 | 4.147 | 3.839 |
| 45 x 15 | 1.2 | 1.35 | 1.06 | 3.089 | 0.536 | 1.515 | 0.631 | 1.373 | 0.715 |
| 45 x 15 | 1.5 | 1.65 | 1.30 | 3.696 | 0.631 | 1.496 | 0.618 | 1.643 | 0.841 |
| 45 x 30 | 1.2 | 1.71 | 1.34 | 4.816 | 2.580 | 1.681 | 1.230 | 2.141 | 1.720 |
| 45 x 30 | 1.5 | 2.10 | 1.65 | 5.826 | 3.111 | 1.665 | 1.216 | 2.589 | 2.074 |
| 45 x 30 | 2.0 | 2.74 | 2.15 | 7.345 | 3.900 | 1.638 | 1.194 | 3.264 | 2.600 |
| 45 x 30 | 3.0 | 3.91 | 3.07 | 9.804 | 5.151 | 1.584 | 1.148 | 4.358 | 3.434 |
| 50 x 10 | 1.0 | 1.13 | 0.89 | 2.885 | 0.206 | 1.595 | 0.426 | 1.154 | 0.412 |
| 50 x 10 | 1.2 | 1.35 | 1.06 | 3.359 | 0.234 | 1.580 | 0.417 | 1.343 | 0.468 |
| 50 x 10 | 1.5 | 1.65 | 1.30 | 4.007 | 0.270 | 1.557 | 0.404 | 1.603 | 0.539 |
| 50 x 10 | 2.0 | 2.14 | 1.68 | 4.926 | 0.312 | 1.518 | 0.382 | 1.970 | 0.624 |
| 50 x 10 | 3.0 | 3.01 | 2.36 | 6.196 | 0.350 | 1.435 | 0.341 | 2.478 | 0.699 |
| 50 x 15 | 1.2 | 1.47 | 1.15 | 4.073 | 0.593 | 1.667 | 0.636 | 1.629 | 0.791 |
| 50 x 15 | 1.5 | 1.80 | 1.41 | 4.889 | 0.699 | 1.647 | 0.623 | 1.956 | 0.933 |
| 50 x 15 | 2.0 | 2.34 | 1.83 | 6.079 | 0.844 | 1.613 | 0.601 | 2.431 | 1.126 |
| 50 x 15 | 3.0 | 3.31 | 2.60 | 7.855 | 1.029 | 1.541 | 0.558 | 3.142 | 1.373 |
| 50 x 25 | 1.0 | 1.43 | 1.13 | 4.686 | 1.605 | 1.808 | 1.058 | 1.875 | 1.284 |
| 50 x 25 | 1.2 | 1.71 | 1.34 | 5.502 | 1.876 | 1.796 | 1.049 | 2.201 | 1.501 |
| 50 x 25 | 1.5 | 2.10 | 1.65 | 6.654 | 2.254 | 1.779 | 1.035 | 2.662 | 1.803 |
| 50 x 25 | 2.0 | 2.74 | 2.15 | 8.384 | 2.809 | 1.750 | 1.013 | 3.354 | 2.247 |
| 50 x 25 | 3.0 | 3.91 | 3.07 | 11.173 | 3.667 | 1.691 | 0.969 | 4.469 | 2.934 |
| 55 x 10 | 2.0 | 2.34 | 1.83 | 6.475 | 0.345 | 1.664 | 0.384 | 2.354 | 0.690 |
| 55 x 10 | 3.0 | 3.31 | 2.60 | 8.264 | 0.389 | 1.580 | 0.343 | 3.005 | 0.777 |
| 55 x 20 | 1.2 | 1.71 | 1.34 | 6.109 | 1.242 | 1.893 | 0.853 | 2.221 | 1.242 |
| 55 x 20 | 1.5 | 2.10 | 1.65 | 7.381 | 1.483 | 1.874 | 0.840 | 2.684 | 1.483 |
| 55 x 20 | 2.0 | 2.74 | 2.15 | 9.285 | 1.831 | 1.842 | 0.818 | 3.376 | 1.831 |
| 55 x 20 | 3.0 | 3.91 | 3.07 | 12.324 | 2.342 | 1.776 | 0.774 | 4.482 | 2.342 |
| 55 x 25 | 1.2 | 1.83 | 1.43 | 6.977 | 2.046 | 1.955 | 1.059 | 2.537 | 1.637 |
| 55 x 25 | 1.5 | 2.25 | 1.77 | 8.454 | 2.461 | 1.938 | 1.045 | 3.074 | 1.969 |
| 55 x 25 | 2.0 | 2.94 | 2.31 | 10.690 | 3.075 | 1.908 | 1.023 | 3.887 | 2.460 |
| 55 x 25 | 3.0 | 4.21 | 3.30 | 14.354 | 4.032 | 1.847 | 0.979 | 5.220 | 3.226 |
| 55 x 35 | 1.2 | 2.07 | 1.62 | 8.714 | 4.354 | 2.054 | 1.452 | 3.169 | 2.488 |
| 55 x 35 | 1.5 | 2.55 | 2.00 | 10.602 | 5.280 | 2.038 | 1.438 | 3.855 | 3.017 |
| 55 x 35 | 2.0 | 3.34 | 2.62 | 13.501 | 6.688 | 2.011 | 1.416 | 4.909 | 3.822 |
| 55 x 35 | 3.0 | 4.81 | 3.77 | 18.415 | 9.029 | 1.957 | 1.370 | 6.696 | 5.160 |
| 55 x 45 | 1.2 | 2.31 | 1.81 | 10.451 | 7.695 | 2.129 | 1.827 | 3.800 | 3.420 |
| 55 x 45 | 1.5 | 2.85 | 2.24 | 12.749 | 9.375 | 2.114 | 1.813 | 4.636 | 4.167 |
| 55 x 45 | 2.0 | 3.74 | 2.93 | 16.311 | 11.971 | 2.089 | 1.790 | 5.931 | 5.320 |
| 55 x 45 | 3.0 | 5.41 | 4.25 | 22.475 | 16.431 | 2.039 | 1.743 | 8.173 | 7.303 |
| 60 x 15 | 1.2 | 1.71 | 1.34 | 6.606 | 0.708 | 1.968 | 0.644 | 2.202 | 0.944 |
| 60 x 15 | 1.5 | 2.10 | 1.65 | 7.969 | 0.837 | 1.947 | 0.631 | 2.656 | 1.116 |
| 60 x 15 | 2.0 | 2.74 | 2.15 | 9.999 | 1.014 | 1.911 | 0.609 | 3.333 | 1.353 |
| 60 x 15 | 3.0 | 3.91 | 3.07 | 13.184 | 1.250 | 1.837 | 0.566 | 4.395 | 1.667 |
| 60 x 20 | 1.2 | 1.83 | 1.43 | 7.643 | 1.348 | 2.046 | 0.859 | 2.548 | 1.348 |
| 60 x 20 | 1.5 | 2.25 | 1.77 | 9.253 | 1.612 | 2.027 | 0.846 | 3.084 | 1.612 |
| 60 x 20 | 2.0 | 2.94 | 2.31 | 11.681 | 1.994 | 1.994 | 0.824 | 3.894 | 1.994 |
| 60 x 20 | 3.0 | 4.21 | 3.30 | 15.623 | 2.561 | 1.927 | 0.780 | 5.208 | 2.561 |
| 60 x 30 | 1.2 | 2.07 | 1.62 | 9.718 | 3.327 | 2.169 | 1.269 | 3.239 | 2.218 |
| 60 x 30 | 1.5 | 2.55 | 2.00 | 11.820 | 4.025 | 2.152 | 1.256 | 3.940 | 2.683 |
| 60 x 30 | 2.0 | 3.34 | 2.62 | 15.047 | 5.078 | 2.123 | 1.234 | 5.016 | 3.385 |
| 60 x 30 | 3.0 | 4.81 | 3.77 | 20.501 | 6.798 | 2.065 | 1.189 | 6.834 | 4.532 |
| 60 x 40 | 1.0 | 1.93 | 1.52 | 9.986 | 5.378 | 2.272 | 1.667 | 3.329 | 2.689 |
| 60 x 40 | 1.2 | 2.31 | 1.81 | 11.792 | 6.340 | 2.262 | 1.658 | 3.931 | 3.170 |
| 60 x 40 | 1.5 | 2.85 | 2.24 | 14.387 | 7.715 | 2.246 | 1.645 | 4.796 | 3.857 |
| 60 x 40 | 2.0 | 3.74 | 2.93 | 18.412 | 9.831 | 2.220 | 1.622 | 6.137 | 4.916 |
| 60 x 40 | 3.0 | 5.41 | 4.25 | 25.379 | 13.440 | 2.166 | 1.576 | 8.460 | 6.720 |
| 60 x 40 | 4.0 | 6.95 | 5.45 | 30.987 | 16.280 | 2.112 | 1.531 | 10.329 | 8.140 |
| 65 x 25 | 1.2 | 2.07 | 1.62 | 10.627 | 2.386 | 2.268 | 1.075 | 3.270 | 1.909 |
| 65 x 25 | 1.5 | 2.55 | 2.00 | 12.919 | 2.876 | 2.250 | 1.062 | 3.975 | 2.301 |
| 65 x 25 | 2.0 | 3.34 | 2.62 | 16.430 | 3.605 | 2.219 | 1.039 | 5.055 | 2.884 |
| 65 x 25 | 3.0 | 4.81 | 3.77 | 22.334 | 4.763 | 2.155 | 0.995 | 6.872 | 3.810 |
| 65 x 25 | 4.0 | 6.15 | 4.83 | 26.832 | 5.567 | 2.089 | 0.952 | 8.256 | 4.454 |
| 65 x 30 | 1.2 | 2.19 | 1.72 | 11.848 | 3.576 | 2.328 | 1.279 | 3.646 | 2.384 |
| 65 x 30 | 1.5 | 2.70 | 2.12 | 14.431 | 4.330 | 2.311 | 1.266 | 4.440 | 2.887 |
| 65 x 30 | 2.0 | 3.54 | 2.78 | 18.415 | 5.471 | 2.282 | 1.244 | 5.666 | 3.647 |
| 65 x 30 | 3.0 | 5.11 | 4.01 | 25.219 | 7.347 | 2.222 | 1.199 | 7.760 | 4.898 |
| 65 x 30 | 4.0 | 6.55 | 5.14 | 30.558 | 8.737 | 2.160 | 1.155 | 9.403 | 5.825 |
| 65 x 35 | 1.2 | 2.31 | 1.81 | 13.069 | 5.040 | 2.381 | 1.479 | 4.021 | 2.880 |
| 65 x 35 | 1.5 | 2.85 | 2.24 | 15.944 | 6.122 | 2.364 | 1.465 | 4.906 | 3.498 |
| 65 x 35 | 2.0 | 3.74 | 2.93 | 20.400 | 7.779 | 2.336 | 1.443 | 6.277 | 4.445 |
| 65 x 35 | 3.0 | 5.41 | 4.25 | 28.105 | 10.570 | 2.280 | 1.398 | 8.648 | 6.040 |
| 65 x 35 | 4.0 | 6.95 | 5.45 | 34.285 | 12.725 | 2.221 | 1.353 | 10.549 | 7.271 |
| 70 x 20 | 1.2 | 2.07 | 1.62 | 11.411 | 1.560 | 2.351 | 0.869 | 3.260 | 1.560 |
| 70 x 20 | 1.5 | 2.55 | 2.00 | 13.861 | 1.869 | 2.330 | 0.856 | 3.960 | 1.869 |
| 70 x 20 | 2.0 | 3.34 | 2.62 | 17.600 | 2.319 | 2.297 | 0.834 | 5.029 | 2.319 |
| 70 x 20 | 3.0 | 4.81 | 3.77 | 23.838 | 2.999 | 2.227 | 0.790 | 6.811 | 2.999 |
| 70 x 20 | 4.0 | 6.15 | 4.83 | 28.508 | 3.428 | 2.153 | 0.747 | 8.145 | 3.428 |
| 70 x 30 | 1.2 | 2.31 | 1.81 | 14.251 | 3.825 | 2.486 | 1.288 | 4.072 | 2.550 |
| 70 x 30 | 1.5 | 2.85 | 2.24 | 17.380 | 4.635 | 2.469 | 1.275 | 4.966 | 3.090 |
| 70 x 30 | 2.0 | 3.74 | 2.93 | 22.225 | 5.863 | 2.439 | 1.253 | 6.350 | 3.909 |
| 70 x 30 | 3.0 | 5.41 | 4.25 | 30.576 | 7.896 | 2.378 | 1.208 | 8.736 | 5.264 |
| 70 x 30 | 4.0 | 6.95 | 5.45 | 37.231 | 9.418 | 2.315 | 1.164 | 10.637 | 6.279 |
| 70 x 50 | 1.2 | 2.79 | 2.19 | 19.932 | 11.934 | 2.675 | 2.070 | 5.695 | 4.773 |
| 70 x 50 | 1.5 | 3.45 | 2.71 | 24.420 | 14.595 | 2.660 | 2.056 | 6.977 | 5.838 |
| 70 x 50 | 2.0 | 4.54 | 3.56 | 31.476 | 18.758 | 2.634 | 2.033 | 8.993 | 7.503 |
| 70 x 50 | 3.0 | 6.61 | 5.19 | 44.052 | 26.104 | 2.582 | 1.987 | 12.586 | 10.441 |
| 70 x 50 | 4.0 | 8.55 | 6.71 | 54.676 | 32.222 | 2.529 | 1.942 | 15.622 | 12.889 |
| 75 x 25 | 1.2 | 2.31 | 1.81 | 15.309 | 2.726 | 2.577 | 1.087 | 4.082 | 2.181 |
| 75 x 25 | 1.5 | 2.85 | 2.24 | 18.660 | 3.290 | 2.558 | 1.074 | 4.976 | 2.632 |
| 75 x 25 | 2.0 | 3.74 | 2.93 | 23.837 | 4.135 | 2.526 | 1.052 | 6.357 | 3.308 |
| 75 x 25 | 3.0 | 5.41 | 4.25 | 32.718 | 5.493 | 2.460 | 1.008 | 8.725 | 4.395 |
| 75 x 25 | 4.0 | 6.95 | 5.45 | 39.726 | 6.460 | 2.391 | 0.964 | 10.594 | 5.168 |
| 75 x 50 | 1.5 | 3.602 | 2.828 | 28.791 | 15.478 | 2.827 | 2.073 | 7.677 | 6.191 |
| 75 x 50 | 2.0 | 4.74 | 3.72 | 37.163 | 19.911 | 2.801 | 2.050 | 9.910 | 7.964 |
| 75 x 50 | 2.5 | 5.84 | 4.58 | 44.951 | 24.001 | 2.775 | 2.027 | 11.987 | 9.601 |
| 75 x 50 | 3.0 | 6.91 | 5.42 | 52.169 | 27.763 | 2.748 | 2.005 | 13.912 | 11.105 |
| 75 x 50 | 4.0 | 8.95 | 7.02 | 64.958 | 34.343 | 2.694 | 1.959 | 17.322 | 13.737 |
| 75 x 50 | 5.0 | 10.86 | 8.52 | 75.651 | 39.747 | 2.640 | 1.913 | 20.174 | 15.899 |
| 80 x 40 | 1.2 | 2.79 | 2.19 | 23.663 | 8.147 | 2.915 | 1.710 | 5.916 | 4.073 |
| 80 x 40 | 1.5 | 3.45 | 2.71 | 28.989 | 9.939 | 2.898 | 1.697 | 7.247 | 4.970 |
| 80 x 40 | 2.0 | 4.54 | 3.56 | 37.358 | 12.722 | 2.869 | 1.675 | 9.339 | 6.361 |
| 80 x 40 | 3.0 | 6.61 | 5.19 | 52.252 | 17.556 | 2.812 | 1.630 | 13.063 | 8.778 |
| 80 x 40 | 4.0 | 8.55 | 6.71 | 64.795 | 21.486 | 2.753 | 1.585 | 16.199 | 10.743 |
| 80 x 60 | 1.5 | 4.05 | 3.18 | 38.233 | 24.656 | 3.072 | 2.467 | 9.558 | 8.219 |
| 80 x 60 | 2.0 | 5.34 | 4.19 | 49.528 | 31.873 | 3.046 | 2.444 | 12.382 | 10.624 |
| 80 x 60 | 3.0 | 7.81 | 6.13 | 70.048 | 44.891 | 2.995 | 2.398 | 17.512 | 14.964 |
| 80 x 60 | 4.0 | 10.15 | 7.97 | 87.920 | 56.117 | 2.943 | 2.352 | 21.980 | 18.706 |
| 90 x 30 | 1.5 | 3.45 | 2.71 | 32.929 | 5.854 | 3.088 | 1.302 | 7.317 | 3.903 |
| 90 x 30 | 2.0 | 4.54 | 3.56 | 42.388 | 7.434 | 3.057 | 1.280 | 9.420 | 4.956 |
| 90 x 30 | 3.0 | 6.61 | 5.19 | 59.136 | 10.092 | 2.991 | 1.236 | 13.141 | 6.728 |
| 90 x 30 | 4.0 | 8.55 | 6.71 | 73.107 | 12.144 | 2.924 | 1.192 | 16.246 | 8.096 |
| 100 x 20 | 1.5 | 3.45 | 2.71 | 35.940 | 2.641 | 3.227 | 0.875 | 7.188 | 2.641 |
| 100 x 20 | 2.0 | 4.54 | 3.56 | 46.167 | 3.295 | 3.190 | 0.852 | 9.233 | 3.295 |
| 100 x 20 | 3.0 | 6.61 | 5.19 | 64.105 | 4.313 | 3.115 | 0.808 | 12.821 | 4.313 |
| 100 x 20 | 4.0 | 8.55 | 6.71 | 78.814 | 4.996 | 3.036 | 0.764 | 15.763 | 4.996 |
| 100 x 40 | 2.0 | 5.34 | 4.19 | 65.377 | 15.612 | 3.500 | 1.710 | 13.075 | 7.806 |
| 100 x 40 | 3.0 | 7.81 | 6.13 | 92.341 | 21.672 | 3.439 | 1.666 | 18.468 | 10.836 |
| 100 x 40 | 4.0 | 10.15 | 7.97 | 115.699 | 26.691 | 3.377 | 1.622 | 23.140 | 13.345 |
| 100 x 50 | 2.5 | 7.09 | 5.56 | 91.205 | 31.059 | 3.587 | 2.093 | 18.241 | 12.424 |
| 100 x 50 | 3.0 | 8.41 | 6.60 | 106.459 | 36.058 | 3.558 | 2.071 | 21.292 | 14.423 |
| 100 x 50 | 4.0 | 10.95 | 8.59 | 134.142 | 44.950 | 3.500 | 2.026 | 26.828 | 17.980 |
| 100 x 50 | 5.0 | 13.36 | 10.48 | 158.190 | 52.455 | 3.441 | 1.982 | 31.638 | 20.982 |
| 100 x 50 | 6.0 | 15.63 | 12.27 | 178.761 | 58.675 | 3.382 | 1.937 | 35.752 | 23.470 |
| 120 x 60 | 3.0 | 10.21 | 8.01 | 189.123 | 64.403 | 4.304 | 2.512 | 31.520 | 21.468 |
| 120 x 60 | 4.0 | 13.35 | 10.48 | 240.745 | 81.248 | 4.247 | 2.467 | 40.124 | 27.083 |
| 120 x 80 | 2.0 | 7.74 | 6.07 | 159.772 | 86.040 | 4.544 | 3.335 | 26.629 | 21.510 |
| 120 x 80 | 2.5 | 9.59 | 7.53 | 195.754 | 105.192 | 4.518 | 3.312 | 32.626 | 26.296 |
| 120 x 80 | 3.0 | 11.41 | 8.96 | 230.199 | 123.436 | 4.492 | 3.289 | 38.366 | 30.859 |
| 120 x 80 | 4.0 | 14.95 | 11.73 | 294.591 | 157.296 | 4.439 | 3.244 | 49.098 | 39.324 |
| 125 x 75 | 3.0 | 11.41 | 8.96 | 242.851 | 110.523 | 4.614 | 3.113 | 38.856 | 29.473 |
| 125 x 75 | 4.0 | 14.95 | 11.73 | 310.771 | 140.653 | 4.560 | 3.067 | 49.723 | 37.507 |
| 125 x 75 | 5.0 | 18.36 | 14.41 | 372.521 | 167.682 | 4.505 | 3.022 | 59.603 | 44.715 |
| 125 x 75 | 6.0 | 21.63 | 16.98 | 428.305 | 191.761 | 4.450 | 2.977 | 68.529 | 51.136 |
| 140 x 60 | 2.0 | 7.74 | 6.07 | 193.130 | 52.065 | 4.996 | 2.594 | 27.590 | 17.355 |
| 140 x 60 | 2.5 | 9.59 | 7.53 | 236.550 | 63.430 | 4.967 | 2.572 | 33.793 | 21.143 |
| 140 x 60 | 3.0 | 11.41 | 8.96 | 278.085 | 74.159 | 4.937 | 2.550 | 39.726 | 24.720 |
| 140 x 60 | 4.0 | 14.95 | 11.73 | 355.602 | 93.813 | 4.877 | 2.505 | 50.800 | 31.271 |
| 150 x 50 | 3.0 | 11.41 | 8.96 | 298.555 | 52.648 | 5.116 | 2.148 | 39.807 | 21.059 |
| 150 x 50 | 4.0 | 14.95 | 11.73 | 381.399 | 66.163 | 5.051 | 2.104 | 50.853 | 26.465 |
| 150 x 50 | 5.0 | 18.36 | 14.41 | 456.299 | 77.872 | 4.986 | 2.060 | 60.840 | 31.149 |
| 150 x 50 | 6.0 | 21.63 | 16.98 | 523.483 | 87.895 | 4.919 | 2.016 | 69.798 | 35.158 |
| 150 x 75 | 3.0 | 12.91 | 10.13 | 379.600 | 129.974 | 5.423 | 3.173 | 50.613 | 34.660 |
| 150 x 75 | 4.0 | 16.95 | 13.30 | 488.006 | 165.884 | 5.366 | 3.129 | 65.067 | 44.236 |
| 150 x 75 | 5.0 | 20.86 | 16.37 | 587.757 | 198.360 | 5.309 | 3.084 | 78.368 | 52.896 |
| 150 x 75 | 6.0 | 24.63 | 19.34 | 679.093 | 227.558 | 5.251 | 3.039 | 90.546 | 60.682 |
| 150 x 100 | 3.0 | 14.41 | 11.31 | 460.645 | 247.639 | 5.654 | 4.146 | 61.419 | 49.528 |
| 150 x 100 | 4.0 | 18.95 | 14.87 | 594.613 | 318.569 | 5.602 | 4.100 | 79.282 | 63.714 |
| 150 x 100 | 5.0 | 23.36 | 18.33 | 719.215 | 384.024 | 5.549 | 4.055 | 95.895 | 76.805 |
| 150 x 100 | 6.0 | 27.63 | 21.69 | 800.121 | 429.761 | 5.381 | 3.944 | 106.683 | 85.952 |
| 150 x 100 | 8.0 | 35.79 | 28.10 | 1,067.14 | 559.76 | 5.46 | 3.95 | 142.29 | 111.95 |
| 200 x 50 | 4.0 | 18.948 | 14.874 | 815.520 | 87.388 | 6.560 | 2.148 | 81.552 | 34.955 |
| 200 x 50 | 5.0 | 23.36 | 18.33 | 983.891 | 103.316 | 6.490 | 2.103 | 98.389 | 41.327 |
| 200 x 50 | 6.0 | 27.63 | 21.69 | 1138.680 | 117.173 | 6.419 | 2.059 | 113.868 | 46.869 |
| 200 x 50 | 8.0 | 35.79 | 28.10 | 1408.746 | 139.249 | 6.274 | 1.972 | 140.875 | 55.700 |
| 200 x 100 | 4.0 | 22.95 | 18.01 | 1199.722 | 410.782 | 7.230 | 4.231 | 119.972 | 82.156 |
| 200 x 100 | 5.0 | 28.36 | 22.26 | 1459.280 | 496.940 | 7.174 | 4.186 | 145.928 | 99.388 |
| 200 x 100 | 6.0 | 33.63 | 26.40 | 1703.342 | 576.921 | 7.116 | 4.142 | 170.334 | 115.384 |
| 200 x 100 | 8.0 | 43.24 | 33.94 | 2,090.91 | 705.37 | 6.95 | 4.04 | 209.09 | 141.07 |
| 200 x 150 | 4.0 | 26.95 | 21.15 | 1583.935 | 1021.039 | 7.667 | 6.155 | 158.394 | 136.139 |
| 200 x 150 | 5.0 | 33.36 | 26.19 | 1934.696 | 1245.049 | 7.616 | 6.109 | 193.470 | 166.006 |
| 200 x 150 | 6.0 | 39.63 | 31.11 | 2268.062 | 1457.143 | 7.565 | 6.063 | 226.806 | 194.286 |
| 200 x 150 | 8.0 | 51.24 | 40.22 | 2,828.62 | 1,815.57 | 7.43 | 5.95 | 282.86 | 242.08 |
| 300 x 100 | 4.0 | 30.95 | 24.29 | 3289.494 | 591.748 | 10.310 | 4.373 | 219.300 | 118.350 |
| 300 x 100 | 5.0 | 38.36 | 30.11 | 4065.277 | 722.774 | 10.295 | 4.341 | 271.018 | 144.555 |
| 300 x 100 | 6.0 | 45.63 | 35.82 | 4776.872 | 842.361 | 10.231 | 4.296 | 318.458 | 168.472 |
| 300 x 100 | 8.0 | 59.24 | 46.50 | 5,978.04 | 1,044.78 | 10.05 | 4.20 | 398.54 | 208.96 |
| 300 x 200 | 4.0 | 38.95 | 30.57 | 5072.923 | 2736.575 | 11.413 | 8.382 | 338.195 | 273.658 |
| 300 x 200 | 5.0 | 48.36 | 37.96 | 6241.110 | 3360.946 | 11.361 | 8.337 | 416.074 | 336.095 |
| 300 x 200 | 6.0 | 57.63 | 45.24 | 7370.312 | 3962.222 | 11.309 | 8.291 | 491.354 | 396.222 |
| 300 x 200 | 8.0 | 75.24 | 59.06 | 9389.451 | 5041.735 | 11.171 | 8.186 | 625.963 | 504.174 |
| 350 x 150 | 4.0 | 38.95 | 30.57 | 6133.375 | 1660.679 | 12.549 | 6.530 | 350.479 | 221.424 |
| 350 x 150 | 5.0 | 48.36 | 37.96 | 7544.127 | 2033.799 | 12.490 | 6.485 | 431.093 | 271.173 |
| 350 x 150 | 6.0 | 57.63 | 45.24 | 8906.982 | 2390.803 | 12.432 | 6.441 | 508.970 | 318.774 |
| 350 x 150 | 8.0 | 75.24 | 59.06 | 11322.126 | 3026.693 | 12.267 | 6.342 | 646.979 | 403.559 |
| 400 x 100 | 6.0 | 57.63 | 45.24 | 10132.070 | 1107.801 | 13.259 | 4.384 | 506.603 | 221.560 |
| 400 x 100 | 8.0 | 75.24 | 59.06 | 12827.344 | 1384.195 | 13.057 | 4.289 | 641.367 | 276.839 |
| Note: Other dimensions and their sectional properties may be produced according to ISO 10799-2 or ISO 12633-2. |  |  |  |  |  |  |  |  |  |

Figure A.3 ― Plain channel section

Table A.3 — Dimensions and properties for cold formed plain channel sections

| Size, B x D mm | Thickness, t mm | Area, A cm2 | Mass, w kg/m | Centroid Y-axis Py cm | Second Moment of area |  | Elastic section modulus |  | Radius of gyration |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Axis x-x Ix cm4 | Axis y-y Iy cm4 | Axis x-x Zx cm3 | Axis y-y Zy cm3 | Axis x-x Rx cm | Axis y-y Ry cm |
| 40 x 25 | 1.5 | 1.305 | 1.024 | 0.750 | 1.430 | 3.414 | 1.907 | 0.171 | 1.047 | 1.617 |
| 40 x 25 | 2.0 | 1.720 | 1.350 | 0.769 | 1.904 | 4.391 | 2.477 | 0.220 | 1.052 | 1.598 |
| 40 x 40 | 1.5 | 1.755 | 1.378 | 1.391 | 5.768 | 5.082 | 4.146 | 0.254 | 1.813 | 1.702 |
| 40 x 40 | 2.0 | 2.320 | 1.821 | 1.410 | 7.681 | 6.559 | 5.446 | 0.328 | 1.820 | 1.681 |
| 50 x 25 | 3.0 | 2.820 | 2.214 | 0.735 | 2.875 | 10.425 | 3.912 | 0.417 | 1.010 | 1.923 |
| 60 x 40 | 3.0 | 4.020 | 3.156 | 1.254 | 11.674 | 23.449 | 9.306 | 0.782 | 1.704 | 2.415 |
| 60x 40 | 4.0 | 5.280 | 4.145 | 1.291 | 15.535 | 29.818 | 12.034 | 0.994 | 1.715 | 2.376 |
| 75 x 40 | 3.0 | 4.470 | 3.509 | 1.143 | 11.779 | 39.335 | 10.303 | 1.049 | 1.623 | 2.966 |
| 75 x 40 | 4.0 | 5.880 | 4.616 | 1.180 | 15.679 | 50.396 | 13.292 | 1.344 | 1.633 | 2.928 |
| 75 x 40 | 4.5 | 6.570 | 5.157 | 1.198 | 17.626 | 55.574 | 14.717 | 1.482 | 1.638 | 2.908 |
| 100 x 50 | 3.0 | 5.820 | 4.569 | 1.361 | 23.090 | 91.355 | 16.961 | 1.827 | 1.992 | 3.962 |
| 100 x 50 | 4.0 | 7.680 | 6.029 | 1.398 | 30.743 | 118.170 | 21.992 | 2.363 | 2.001 | 3.923 |
| 100 x 50 | 4.5 | 8.595 | 6.747 | 1.416 | 34.563 | 130.938 | 24.407 | 2.619 | 2.005 | 3.903 |
| 100 x 50 | 6.0 | 11.280 | 8.855 | 1.470 | 46.007 | 166.794 | 31.293 | 3.336 | 2.020 | 3.845 |
| 120 x 50 | 3.0 | 6.420 | 5.040 | 1.248 | 23.256 | 139.729 | 18.633 | 2.329 | 1.903 | 4.665 |
| 120 x 50 | 4.0 | 8.480 | 6.657 | 1.285 | 30.969 | 181.444 | 24.102 | 3.024 | 1.911 | 4.626 |
| 120 x 50 | 6.0 | 12.480 | 9.797 | 1.358 | 46.365 | 258.106 | 34.150 | 4.302 | 1.927 | 4.548 |
| 120 x 65 | 4.5 | 10.845 | 8.513 | 1.857 | 75.799 | 246.486 | 40.824 | 4.108 | 2.644 | 4.767 |
| 125 x 65 | 4.0 | 9.880 | 7.756 | 1.805 | 67.526 | 243.789 | 37.405 | 3.901 | 2.614 | 4.967 |
| 125 x 65 | 6.0 | 14.580 | 11.445 | 1.878 | 101.071 | 348.518 | 53.813 | 5.576 | 2.633 | 4.889 |
| 150 x 50 | 6.0 | 14.280 | 11.210 | 1.224 | 46.800 | 442.624 | 38.224 | 5.902 | 1.810 | 5.567 |
| 150 x 70 | 4.0 | 11.280 | 8.855 | 1.838 | 84.728 | 393.942 | 46.091 | 5.253 | 2.741 | 5.910 |
| 150 x 70 | 6.0 | 16.680 | 13.094 | 1.912 | 126.844 | 567.112 | 66.358 | 7.561 | 2.758 | 5.831 |
| 150 x 75 | 4.0 | 11.680 | 9.169 | 2.024 | 103.961 | 415.263 | 51.373 | 5.537 | 2.983 | 5.963 |
| 150 x 75 | 6.0 | 17.280 | 13.565 | 2.097 | 155.636 | 598.234 | 74.223 | 7.976 | 3.001 | 5.884 |
| 200 x 75 | 4.5 | 15.345 | 12.046 | 1.776 | 118.215 | 906.376 | 66.578 | 9.064 | 2.776 | 7.685 |
| 200 x 75 | 4.0 | 13.680 | 10.739 | 1.757 | 105.128 | 812.250 | 59.833 | 8.122 | 2.772 | 7.706 |
| 200 x 75 | 5.0 | 17.000 | 13.345 | 1.794 | 131.294 | 998.917 | 73.180 | 9.989 | 2.779 | 7.665 |
| 200 x 75 | 6.0 | 20.280 | 15.920 | 1.831 | 157.433 | 1179.314 | 85.979 | 11.793 | 2.786 | 7.626 |
| 200 x 100 | 6.0 | 23.280 | 18.275 | 2.723 | 369.445 | 1461.674 | 135.692 | 14.617 | 3.984 | 7.924 |

Figure A.4 ― Plain equal angles section

Table A.4 — Dimensions and properties for cold formed plain equal angles sections

| Size, B × D mm | Thickness, t mm | Cross sectional area, A cm2 | Mass, w kg/m | Centroid, P cm | Axis X-X |  |  | Axis Y-Y |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Ix cm4 | Zx cm3 | Rx cm | Iy cm4 | Zy cm3 | Ry cm |
| 20 x 20 | 2.5 | 0.888 | 0.69 | 1.10 | 0.33 | 0.24 | 0.614 | 0.33 | 0.23 | 0.614 |
| 25 x 25 | 2.5 | 1.13 | 0.89 | 0.75 | 0.68 | 0.39 | 0.775 | 0.68 | 0.38 | 0.775 |
| 25 x 25 | 2.0 | 1.65 | 1.09 | 0.70 | 0.42 | 1.06 | 1.12 | 0.42 | 1.06 | 1.12 |
| 25 x 25 | 3 | 1.33 | 1.05 | 0.78 | 0.80 | 0.46 | 0.773 | 0.80 | 0.46 | 0.773 |
| 30 x 30 | 2.0 | 1.23 | 1.10 | 0.84 | 1.10 | 1.05 | 1.09 | 1.10 | 1.05 | 1.09 |
| 30 x 30 | 2.5 | 1.38 | 1.08 | 0.87 | 1.24 | 0.58 | 0.941 | 1.24 | 0.58 | 0.941 |
| 30 x 30 | 3 | 1.63 | 1.28 | 0.90 | 1.43 | 0.68 | 0.935 | 1.43 | 0.68 | 0.935 |
| 32 x 32 | 3 | 1.74 | 1.37 | 0.91 | 1.54 | 0.67 | 0.94 | 1.54 | 0.67 | 0.94 |
| 32 x 32 | 4 | 2.24 | 1.76 | 0.898 | 1.86 | 0.81 | 0.91 | 1.86 | 0.81 | 0.91 |
| 32 x 32 | 4.5 | 2.48 | 1.88 | 0.906 | 1.99 | 0.87 | 0.90 | 1.99 | 0.87 | 0.90 |
| 32 x 32 | 6 | 3.12 | 2.45 | 1.03 | 2.30 | 1.06 | 0.86 | 2.30 | 1.06 | 0.86 |
| 40 x 40 | 2.0 | 1.46 | 1.14 | 1.09 | 2.46 | 1.23 | 1.21 | 2.46 | 1.23 | 1.21 |
| 40 x 40 | 2.5 | 1.88 | 1.47 | 1.13 | 2.96 | 1.03 | 1.25 | 2.96 | 1.03 | 1.25 |
| 40 x 40 | 3 | 2.22 | 1.74 | 1.06 | 3.18 | 1.08 | 1.20 | 3.18 | 1.08 | 1.20 |
| 40 x 40 | 4 | 2.88 | 2.26 | 1.097 | 3.92 | 1.32 | 1.17 | 3.92 | 1.32 | 1.17 |
| 40 x 40 | 4.5 | 3.20 | 2.51 | 1.11 | 4.24 | 1.47 | 1.15 | 4.24 | 1.47 | 1.15 |
| 40 x 40 | 6 | 4.08 | 3.20 | 1.23 | 5.66 | 2.04 | 1.18 | 5.66 | 2.04 | 1.18 |
| 50 x 50 | 2.0 | 1.86 | 1.46 | 1.34 | 4.85 | 1.33 | 1.59 | 4.85 | 1.33 | 1.59 |
| 50 x 50 | 3 | 2.83 | 2.22 | 1.40 | 7.01 | 1.94 | 1.57 | 7.01 | 1.94 | 1.57 |
| 50 x 50 | 4 | 3.70 | 2.90 | 1.45 | 8.89 | 2.50 | 1.56 | 8.89 | 2.50 | 1,56 |
| 50 x 50 | 4.4 | 4.10 | 3.22 | 1.42 | 8.91 | 2.49 | 1.47 | 8.91 | 2.49 | 1.47 |
| 50 x 50 | 6 | 5.28 | 4.14 | 1.48 | 12.43 | 3.53 | 1.53 | 12.43 | 3.53 | 1.53 |
| 60 x 60 | 4 | 4.50 | 3.53 | 1.68 | 16.01 | 3.70 | 1.88 | 16.01 | 3.70 | 1.88 |
| 60 x 60 | 6 | 6.53 | 5.13 | 1.80 | 22.55 | 5.37 | 1.87 | 22.55 | 5.37 | 1.87 |
| 65 x 65 | 4.5 | 5.45 | 4.28 | 1.79 | 19.03 | 4.04 | 1.87 | 19.03 | 4.04 | 1.87 |
| 65 x 65 | 6 | 7.08 | 5.56 | 1.85 | 25.90 | 5.57 | 1.91 | 25.90 | 5.57 | 1.91 |
| 75 x 75 | 6 | 8.69 | 6.78 | 2.09 | 46.88 | 8.67 | 2.33 | 46.88 | 8.67 | 2.33 |
| 90 x 90 | 6 | 10.08 | 7.91 | 2.48 | 74.42 | 11.41 | 2.72 | 74.42 | 11.41 | 2.72 |
| 100 x 100 | 6 | 11.30 | 8.87 | 2.80 | 112.59 | 15.59 | 3.15 | 112.28 | 15.59 | 3.15 |

Figure A.5 — Plain unequal angles

Table A.5 — Dimensions and properties for cold formed plain unequal angle sections

| Size, B x D mm | Thickness, t mm | Area, A cm2 | Mass, w kg/m | Centroid |  | Axis, x-x |  |  | Axis, y-y |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Px cm | Py cm | Ix cm4 | zx cm3 | rx cm | Iy cm4 | zy cm3 | ry cm |
| 50 x 40 | 6.0 | 4.65 | 3.67 | 1.53 | 1.11 | 9.96 | 2.87 | 1.04 | 5.41 | 1.83 | 1.08 |
| 65 x 50 | 6.0 | 6.18 | 4.85 | 1.99 | 1.31 | 11.68 | 2.59 | 1.24 | 11.74 | 3.12 | 1.38 |
| 75 x 50 | 6.0 | 6.78 | 5.32 | 2.40 | 1.22 | 35.81 | 7.02 | 1.15 | 17.58 | 4.57 | 1.61 |
| 90 x 65 | 6.0 | 8.58 | 6.73 | 2.76 | 1.59 | 66.56 | 10.67 | 1.51 | 28.58 | 5.73 | 1.83 |
| 90 x 75 | 6.0 | 9.78 | 7.61 | 3.01 | 1.93 | 94.54 | 13.53 | 1.76 | 45.09 | 7.86 | 2.15 |

Figure A.6 ― Cold formed outwardly lipped channel section

Table A.6 — Dimensions and properties for cold formed outwardly lipped channel sections

| Size mm |  |  | Thickness, t mm | Area, A cm2 | Mass, w kg/m | Centroid, p cm | Axis x-x |  |  | Axis y-y |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B | D | C |  |  |  |  | Ix cm4 | zx cm3 | rx cm | Iy cm4 | zy cm3 | ry cm |
| 20 | 20 | 10 | 1.5 | 1.20 | 0.94 | 1.116 | 0.6860 | 0.610 | 1.75 | 1.7260 | 1.730 | 1.195 |
| 20 | 20 | 15 | 2.0 | 1.54 | 1.20 | 1.118 | 0.7910 | 0.710 | 0.72 | 2.1300 | 0.930 | 1.180 |
| 25 | 25 | 15 | 1.5 | 1.43 | 1.12 | 1.305 | 1.2900 | 0.990 | 0.95 | 2.6540 | 1.020 | 1.363 |
| 25 | 25 | 15 | 2.0 | 1.84 | 1.44 | 1.313 | 1.5630 | 0.920 | 0.92 | 3.3000 | 1.290 | 1.340 |
| 40 | 25 | 15 | 1.5 | 1.88 | 1.47 | 2.077 | 4.0470 | 1.950 | 1.47 | 3.2760 | 1.260 | 1.321 |
| 40 | 25 | 15 | 2.0 | 2.44 | 1.91 | 2.078 | 5.0220 | 2.410 | 1.44 | 4.0900 | 1.600 | 1.295 |
| 50 | 50 | 20 | 1.5 | 2.70 | 2.12 | 2.366 | 10.0800 | 3.820 | 1.93 | 16.4500 | 3.780 | 2.467 |
| 50 | 50 | 20 | 2.0 | 3.54 | 2.77 | 2.365 | 12.8000 | 3.850 | 1.90 | 21.0600 | 4.900 | 2.442 |
| 75 | 50 | 20 | 2.0 | 4.74 | 3.71 | 3.590 | 36.9700 | 9.850 | 2.79 | 31.0100 | 6.460 | 2.559 |
| 75 | 50 | 20 | 2.5 | 5.84 | 4.58 | 3.588 | 44.5700 | 11.880 | 2.76 | 37.4300 | 7.880 | 2.532 |
| 75 | 50 | 20 | 3.0 | 6.91 | 5.42 | 3.586 | 51.5600 | 13.740 | 2.73 | 43.4000 | 9.230 | 2.507 |
| 100 | 50 | 30 | 2.0 | 5.93 | 4.66 | 5.166 | 79.3600 | 15.360 | 3.66 | 41.8500 | 7.890 | 2.657 |
| 100 | 50 | 30 | 2.5 | 7.33 | 5.76 | 5.167 | 96.400 | 18.650 | 3.63 | 50.7400 | 9.660 | 2.631 |
| 100 | 50 | 30 | 3.0 | 8.70 | 6.28 | 5.166 | 112.40000 | 21.750 | 3.60 | 59.0600 | 11.350 | 2.605 |

Figure A.7 ― Circular tubes

Table A.7 — Dimensions and properties for cold formed circular tubes

| Diameter, D mm | Thickness, t mm | Area, A cm2 | Mass, w kg/m | Second Moment of Area, I cm4 | Radius of gyration, r cm | Elastic section modulus, z cm3 |
| --- | --- | --- | --- | --- | --- | --- |
| 10 | 1.00 | 0.28 | 0.22 | 0.0290 | 0.3202 | 0.06 |
| 10 | 1.20 | 0.33 | 0.26 | 0.0327 | 0.3140 | 0.07 |
| 10 | 1.50 | 0.40 | 0.31 | 0.0373 | 0.3052 | 0.07 |
| 12 | 1.00 | 0.35 | 0.27 | 0.0527 | 0.3905 | 0.09 |
| 12 | 1.20 | 0.41 | 0.32 | 0.0601 | 0.3842 | 0.10 |
| 12 | 1.50 | 0.49 | 0.39 | 0.0696 | 0.3750 | 0.12 |
| 16 | 1.00 | 0.47 | 0.37 | 0.1331 | 0.5315 | 0.17 |
| 16 | 1.20 | 0.56 | 0.44 | 0.1538 | 0.5250 | 0.19 |
| 16 | 1.50 | 0.68 | 0.54 | 0.1815 | 0.5154 | 0.23 |
| 16 | 2.00 | 0.88 | 0.69 | 0.2199 | 0.5000 | 0.27 |
| 20 | 1.00 | 0.60 | 0.47 | 0.2701 | 0.6727 | 0.27 |
| 20 | 1.20 | 0.71 | 0.56 | 0.3144 | 0.6660 | 0.31 |
| 20 | 1.50 | 0.87 | 0.68 | 0.3755 | 0.6562 | 0.38 |
| 20 | 2.00 | 1.13 | 0.89 | 0.4638 | 0.6403 | 0.46 |
| 22 | 1.00 | 0.66 | 0.52 | 0.3646 | 0.7433 | 0.33 |
| 22 | 1.20 | 0.78 | 0.62 | 0.4255 | 0.7366 | 0.39 |
| 22 | 1.50 | 0.97 | 0.76 | 0.5103 | 0.7267 | 0.46 |
| 22 | 2.00 | 1.26 | 0.99 | 0.6347 | 0.7106 | 0.58 |
| 25 | 1.00 | 0.75 | 0.59 | 0.5439 | 0.8493 | 0.44 |
| 25 | 1.20 | 0.90 | 0.70 | 0.6370 | 0.8425 | 0.51 |
| 25 | 1.50 | 1.11 | 0.87 | 0.7677 | 0.8325 | 0.61 |
| 25 | 2.00 | 1.45 | 1.13 | 0.9629 | 0.8162 | 0.77 |
| 28 | 1.00 | 0.85 | 0.67 | 0.7741 | 0.9552 | 0.55 |
| 28 | 1.20 | 1.01 | 0.79 | 0.9090 | 0.9485 | 0.65 |
| 28 | 1.50 | 1.25 | 0.98 | 1.0999 | 0.9384 | 0.79 |
| 28 | 2.00 | 1.63 | 1.28 | 1.3888 | 0.9220 | 0.99 |
| 30 | 1.00 | 0.91 | 0.72 | 0.9590 | 1.0259 | 0.64 |
| 30 | 1.20 | 1.09 | 0.85 | 1.1278 | 1.0191 | 0.75 |
| 30 | 1.50 | 1.34 | 1.05 | 1.3676 | 1.0090 | 0.91 |
| 30 | 2.00 | 1.76 | 1.38 | 1.7331 | 0.9925 | 1.16 |
| 30 | 3.00 | 2.55 | 2.00 | 2.3478 | 0.9605 | 1.57 |
| 32 | 1.00 | 0.97 | 0.76 | 1.1713 | 1.0966 | 0.73 |
| 32 | 1.20 | 1.16 | 0.91 | 1.3791 | 1.0898 | 0.86 |
| 32 | 1.50 | 1.44 | 1.13 | 1.6755 | 1.0796 | 1.05 |
| 32 | 2.00 | 1.89 | 1.48 | 2.1303 | 1.0630 | 1.33 |
| 32 | 3.00 | 2.73 | 2.15 | 2.9044 | 1.0308 | 1.82 |
| 38 | 1.00 | 1.16 | 0.91 | 1.9908 | 1.3086 | 1.05 |
| 38 | 1.20 | 1.39 | 1.09 | 2.3513 | 1.3018 | 1.24 |
| 38 | 1.50 | 1.72 | 1.35 | 2.8696 | 1.2916 | 1.51 |
| 38 | 2.00 | 2.26 | 1.78 | 3.6761 | 1.2748 | 1.93 |
| 38 | 3.00 | 3.30 | 2.59 | 5.0889 | 1.2420 | 2.68 |
| 42 | 1.00 | 1.29 | 1.01 | 2.7085 | 1.4500 | 1.29 |
| 42 | 1.20 | 1.54 | 1.21 | 3.2037 | 1.4431 | 1.53 |
| 42 | 1.50 | 1.91 | 1.50 | 3.9189 | 1.4329 | 1.87 |
| 42 | 2.00 | 2.51 | 1.97 | 5.0398 | 1.4160 | 2.40 |
| 42 | 3.00 | 3.68 | 2.89 | 7.0306 | 1.3829 | 3.35 |
| 45 | 1.00 | 1.38 | 1.09 | 3.3473 | 1.5560 | 1.49 |
| 45 | 1.20 | 1.65 | 1.30 | 3.9632 | 1.5491 | 1.76 |
| 45 | 1.50 | 2.05 | 1.61 | 4.8550 | 1.5389 | 2.16 |
| 45 | 2.00 | 2.70 | 2.12 | 6.2588 | 1.5219 | 2.78 |
| 45 | 3.00 | 3.96 | 3.11 | 8.7740 | 1.4887 | 3.90 |
| 48 | 1.00 | 1.48 | 1.16 | 4.0795 | 1.6621 | 1.70 |
| 48 | 1.20 | 1.76 | 1.39 | 4.8342 | 1.6552 | 2.01 |
| 48 | 1.50 | 2.19 | 1.72 | 5.9295 | 1.6449 | 2.47 |
| 48 | 2.00 | 2.89 | 2.27 | 7.6602 | 1.6279 | 3.19 |
| 48 | 3.00 | 4.24 | 3.33 | 10.7845 | 1.5945 | 4.49 |
| 50 | 1.20 | 1.84 | 1.44 | 5.4805 | 1.7259 | 2.19 |
| 50 | 1.50 | 2.29 | 1.79 | 6.7274 | 1.7156 | 2.69 |
| 50 | 2.00 | 3.02 | 2.37 | 8.7021 | 1.6985 | 3.48 |
| 50 | 3.00 | 4.43 | 3.48 | 12.2828 | 1.6651 | 4.91 |
| 51 | 1.00 | 1.57 | 1.23 | 4.9113 | 1.7681 | 1.93 |
| 51 | 1.20 | 1.88 | 1.47 | 5.8242 | 1.7612 | 2.28 |
| 51 | 1.50 | 2.33 | 1.83 | 7.1519 | 1.7509 | 2.80 |
| 51 | 2.00 | 3.08 | 2.42 | 9.2567 | 1.7339 | 3.63 |
| 51 | 3.00 | 4.52 | 3.55 | 13.0814 | 1.7004 | 5.13 |
| 57 | 1.20 | 2.10 | 1.65 | 8.1922 | 1.9733 | 2.87 |
| 57 | 1.50 | 2.62 | 2.05 | 10.0787 | 1.9629 | 3.54 |
| 57 | 2.00 | 3.46 | 2.71 | 13.0860 | 1.9458 | 4.59 |
| 57 | 3.00 | 5.09 | 4.00 | 18.6105 | 1.9121 | 6.53 |
| 60 | 1.20 | 2.22 | 1.74 | 9.5854 | 2.0793 | 3.20 |
| 60 | 1.50 | 2.76 | 2.16 | 11.8021 | 2.0690 | 3.93 |
| 60 | 2.00 | 3.64 | 2.86 | 15.3443 | 2.0518 | 5.11 |
| 60 | 3.00 | 5.37 | 4.22 | 21.8808 | 2.0180 | 7.29 |
| 63 | 1.20 | 2.33 | 1.83 | 11.1282 | 2.1854 | 3.53 |
| 63 | 1.50 | 2.90 | 2.28 | 13.7117 | 2.1750 | 4.35 |
| 63 | 2.00 | 3.83 | 3.01 | 17.8485 | 2.1578 | 5.67 |
| 63 | 3.00 | 5.66 | 4.44 | 25.5138 | 2.1240 | 8.10 |
| 76 | 1.50 | 3.51 | 2.76 | 24.3698 | 2.6345 | 6.41 |
| 76 | 2.00 | 4.65 | 3.65 | 31.8536 | 2.6173 | 8.38 |
| 76 | 3.00 | 6.88 | 5.40 | 45.9133 | 2.5831 | 12.08 |
| 89 | 2.00 | 5.47 | 4.29 | 51.7527 | 3.0767 | 11.63 |
| 89 | 3.00 | 8.11 | 6.36 | 75.0345 | 3.0424 | 16.86 |
| 89 | 3.25 | 8.76 | 6.87 | 80.5982 | 3.0339 | 18.11 |
| 89 | 4.00 | 10.68 | 8.39 | 96.6927 | 3.0085 | 21.73 |
| 89 | 4.85 | 12.82 | 10.07 | 113.8834 | 2.9801 | 25.59 |
| 100 | 2.00 | 6.16 | 4.83 | 73.9614 | 3.4655 | 14.79 |
| 100 | 3.00 | 9.14 | 7.18 | 107.6386 | 3.4311 | 21.53 |
| 100 | 4.00 | 12.07 | 9.47 | 139.2333 | 3.3971 | 27.85 |
| 114 | 2.00 | 7.04 | 5.52 | 110.3923 | 3.9604 | 19.37 |
| 114 | 3.00 | 10.46 | 8.21 | 161.2588 | 3.9259 | 28.29 |
| 114 | 5.00 | 17.12 | 13.44 | 254.8464 | 3.8578 | 44.71 |
| 114 | 6.00 | 20.36 | 15.98 | 297.7673 | 3.8243 | 52.24 |
| 127 | 3.00 | 11.69 | 9.18 | 224.7795 | 4.3853 | 35.40 |
| 127 | 4.00 | 15.46 | 12.14 | 292.6514 | 4.3510 | 46.09 |
| 127 | 5.00 | 19.17 | 15.05 | 357.1861 | 4.3170 | 56.25 |
| 127 | 6.00 | 22.81 | 17.91 | 418.4948 | 4.2833 | 65.90 |
| 140 | 3.00 | 12.91 | 10.14 | 303.1149 | 4.8448 | 43.30 |
| 140 | 4.00 | 17.09 | 13.42 | 395.5200 | 4.8104 | 56.50 |
| 140 | 5.00 | 21.21 | 16.65 | 483.8189 | 4.7762 | 69.12 |
| 140 | 6.00 | 25.26 | 19.83 | 568.1352 | 4.7424 | 81.16 |
| 152 | 3.00 | 14.04 | 11.03 | 389.9171 | 5.2690 | 51.30 |
| 152 | 4.00 | 18.60 | 14.60 | 509.6575 | 5.2345 | 67.06 |
| 165 | 3.00 | 15.27 | 11.99 | 501.1081 | 5.7285 | 60.74 |
| 165 | 4.00 | 20.23 | 15.88 | 656.0271 | 5.6940 | 79.52 |
| 165 | 4.85 | 24.40 | 19.16 | 783.1354 | 5.6648 | 94.93 |
| 216 | 5.00 | 33.15 | 26.02 | 1,845.7691 | 7.4621 | 170.90 |
| 216 | 6.00 | 39.59 | 31.08 | 2,184.1362 | 7.4277 | 202.23 |
| 216 | 7.00 | 45.97 | 36.08 | 2,512.6963 | 7.3934 | 232.66 |
| Note: Other dimensions and their sectional properties may be produced according to ISO 10799-2 or ISO 12633-2. |  |  |  |  |  |  |

Figure A.8 ― Zed purlins

Table A.8 — Dimensions and properties for cold formed structural steel zed purlins

| Dimension mm |  |  | Thickness mm | Area cm2 | Mass per metre run kg/m | Centroid cm |  | Moment of Inertia cm4 |  | Section modulus of elasticity cm3 |  | Radius of gyration cm |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B | D | C | t | A | W | CX | Cy | IXX | IYY | ZXX | ZYY | RXX | RYY |
| 50 | 75 | 20 | 1.5 | 3.135 | 2.461 | 3.75 | 5 | 33.594 | 61.256 | 6.719 | 16.335 | 3.2735 | 4.4203 |
| 50 | 75 | 20 | 2.0 | 4.14 | 3.250 | 3.75 | 5 | 43.917 | 77.754 | 8.783 | 20.734 | 3.2570 | 4.3337 |
| 50 | 100 | 20 | 2.0 | 4.64 | 3.642 | 5 | 5 | 86.718 | 77.755 | 17.344 | 15.551 | 4.3231 | 4.0936 |
| 50 | 113 | 20 | 2.0 | 4.9 | 3.847 | 5.65 | 5 | 115.594 | 77.756 | 23.119 | 13.762 | 4.8570 | 3.9835 |
| 50 | 125 | 20 | 2.0 | 5.14 | 4.035 | 6.25 | 5 | 146.518 | 77.757 | 29.304 | 12.441 | 5.3391 | 3.8895 |
| 50 | 138 | 20 | 2.0 | 5.4 | 4.239 | 6.9 | 5 | 184.852 | 77.758 | 36.970 | 11.269 | 5.8508 | 3.7947 |
| 50 | 150 | 20 | 2.0 | 5.64 | 4.427 | 7.5 | 5 | 224.881 | 77.759 | 44.976 | 10.368 | 6.3145 | 3.7131 |
| 50 | 150 | 20 | 2.5 | 7 | 5.495 | 7.5 | 5 | 277.536 | 92.451 | 55.507 | 12.327 | 6.2967 | 3.6342 |
| 50 | 163 | 20 | 2.0 | 5.9 | 4.632 | 8.15 | 5 | 273.485 | 77.760 | 54.697 | 9.541 | 6.8083 | 3.6304 |
| 50 | 163 | 20 | 2.5 | 7.325 | 5.750 | 8.15 | 5 | 337.715 | 92.452 | 67.543 | 11.344 | 6.7900 | 3.5527 |
| 50 | 175 | 20 | 2.0 | 6.14 | 4.820 | 8.75 | 5 | 323.369 | 77.760 | 64.674 | 8.887 | 7.2571 | 3.5587 |
| 50 | 175 | 20 | 2.5 | 7.625 | 5.986 | 8.75 | 5 | 399.503 | 92.454 | 79.901 | 10.566 | 7.2384 | 3.4821 |
| 63 | 175 | 20 | 2.0 | 6.66 | 5.228 | 8.75 | 6.3 | 362.279 | 147.516 | 57.505 | 16.859 | 7.3754 | 4.7063 |
| 63 | 175 | 20 | 2.5 | 8.275 | 6.496 | 8.75 | 6.3 | 447.860 | 177.244 | 71.089 | 20.256 | 7.3568 | 4.6281 |
| 75 | 175 | 20 | 3.0 | 10.59 | 8.313 | 8.75 | 7.5 | 584.760 | 336.506 | 77.968 | 38.458 | 7.4309 | 5.6370 |
| 50 | 200 | 20 | 2.0 | 6.64 | 5.212 | 10 | 5 | 443.545 | 77.762 | 88.709 | 7.776 | 8.1731 | 3.4222 |
| 50 | 200 | 20 | 2.5 | 8.25 | 6.476 | 10 | 5 | 548.422 | 92.457 | 109.684 | 9.246 | 8.1532 | 3.3477 |
| 75 | 200 | 20 | 2.5 | 9.5 | 7.458 | 10 | 7.5 | 670.323 | 290.003 | 89.376 | 29.000 | 8.4000 | 5.5251 |
| 75 | 200 | 20 | 3.0 | 11.34 | 8.902 | 10 | 7.5 | 796.504 | 336.512 | 106.201 | 33.651 | 8.3808 | 5.4475 |
| 50 | 225 | 20 | 2.0 | 7.14 | 5.605 | 11.25 | 5 | 586.970 | 77.764 | 117.394 | 6.912 | 9.0669 | 3.3002 |
| 50 | 225 | 20 | 2.5 | 8.875 | 6.967 | 11.25 | 5 | 726.247 | 92.460 | 145.249 | 8.219 | 9.0460 | 3.2277 |
| 50 | 225 | 20 | 3.0 | 10.59 | 8.313 | 11.25 | 5 | 862.610 | 105.437 | 172.522 | 9.372 | 9.0252 | 3.1554 |
| 75 | 225 | 20 | 2.0 | 8.14 | 6.390 | 11.25 | 7.5 | 711.296 | 239.830 | 94.839 | 21.318 | 9.3479 | 5.4280 |
| 75 | 225 | 20 | 2.5 | 10.125 | 7.948 | 11.25 | 7.5 | 880.961 | 290.006 | 117.461 | 25.778 | 9.3278 | 5.3519 |
| 75 | 225 | 20 | 3.0 | 12.09 | 9.491 | 11.25 | 7.5 | 1047.436 | 336.517 | 139.658 | 29.913 | 9.3079 | 5.2758 |
| 50 | 250 | 20 | 2.0 | 7.64 | 5.997 | 12.5 | 5 | 755.208 | 77.765 | 151.042 | 6.221 | 9.9423 | 3.1904 |
| 50 | 250 | 20 | 2.5 | 9.5 | 7.458 | 12.5 | 5 | 934.932 | 92.464 | 186.986 | 7.397 | 9.9204 | 3.1198 |
| 50 | 250 | 20 | 3.0 | 11.34 | 8.902 | 12.5 | 5 | 1111.104 | 105.443 | 222.221 | 8.435 | 9.8985 | 3.0493 |
| 75 | 250 | 20 | 2.0 | 8.64 | 6.782 | 12.5 | 7.5 | 908.971 | 239.831 | 121.196 | 19.187 | 10.2569 | 5.2686 |
| 75 | 250 | 20 | 2.5 | 10.75 | 8.439 | 12.5 | 7.5 | 1126.365 | 290.009 | 150.182 | 23.201 | 10.2361 | 5.1940 |
| 75 | 250 | 20 | 3.0 | 12.84 | 10.079 | 12.5 | 7.5 | 1339.899 | 336.523 | 178.653 | 26.922 | 10.2154 | 5.1195 |

Figure A.9 ― Cold formed mono rail sections

Table A.9 — Dimensions and properties or cold formed steel mono rail sections

| Dimension mm |  |  |  |  | Thickness mm |  | Area cm2 |  | Mass kg/m |  | Axis x-x |  |  |  | Axis y-y |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B | D | C | C1 | E |  | t |  | A |  | w |  | Ix cm4 | zx cm3 | rx cm |  | Iy cm4 | zy cm3 | rx cm |
| 57 | 67 | 15.0 | 10.0 | 13.7 |  | 3.0 |  | 6.27 |  | 4.92 |  | 34.3400 | 9.190 | 2.34 |  | 31.6300 | 11.100 | 2.25 |
| 42 | 54 | 12.5 | 8.0 | 8.0 |  | 2.5 |  | 3.97 |  | 3.12 |  | 14.35000 | 4.640 | 1.90 |  | 11.1100 | 5.290 | 1.67 |
| 33 | 34 | 9.5 | 6.5 | 10.5 |  | 2.0 |  | 2.22 |  | 1.74 |  | 3.2200 | 1.650 | 1.20 |  | 3.6700 | 2.220 | 1.28 |

Figure A.10 ― Bottle sections

Table A.10 — Dimensions and properties of cold formed steel bottle sections

| Nominal size mm | Dimension mm |  |  |  |  |  | Thickness mm | Mass kg/m |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | B | C | D | E | F | G | t | w |
| 94 | 34 | 64 | 30 | 15 | 2 | 15 | 1.0 | 1.74 |
| 94 | 34 | 64 | 30 | 15 | 2 | 15 | 1.2 | 2.10 |
| 94 | 34 | 64 | 30 | 15 | 2 | 15 | 1.5 | 2.60 |
| 94 | 34 | 64 | 30 | 15 | 2 | 15 | 2.0 | 3.50 |

Figure A.11 ― Door frame

Table A.11 — Dimensions and properties of cold formed steel door frame sections

| Nominal size mm | Dimension mm |  |  |  |  |  | Thickness mm | Mass kg/m |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | B | C | D | E | F | G/H | t | w |
| 150 | 48 | 54 | 48 | 13 | 30.00 | 12.00 | 1.0 | 1.9 |
| 130 | 45 | 50 | 35 | 15.00 | 30.15 | 15.15 | 1.0 | 1.8 |
| 130 | 45 | 50 | 35 | 15.00 | 30.15 | 15.15 | 1.2 | 2.1 |
| 130 | 45 | 50 | 35 | 15.00 | 30.15 | 15.15 | 1.5 | 2.6 |
| 130 | 45 | 50 | 35 | 15.00 | 30.15 | 15.15 | 2.0 | 3.5 |

Figure A.12 — Half door frame section

Table A.12 — Dimensions and properties of cold formed steel door frame section

| Dimension mm |  |  |  |  |  |  | Thickness mm |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A | B | C | D | E | F | G |  |
| 95 | 50 | 45 | 42 | 15 | 30 | 11 | 1.0 |
| 95 | 50 | 45 | 42 | 15 | 30 | 11 | 1.2 |
| 95 | 50 | 45 | 42 | 15 | 30 | 11 | 1.5 |
| 100 | 48 | 52 | 42 | 12 | 29 | 13 | 1.0 |
| 100 | 48 | 52 | 42 | 12 | 29 | 13 | 1.2 |
| 100 | 48 | 52 | 42 | 12 | 29 | 13 | 1.5 |
| 105 | 60 | 45 | 60 | 15 | 45 | 12 | 1.0 |
| 105 | 60 | 45 | 60 | 15 | 45 | 12 | 1.2 |
| 105 | 60 | 45 | 60 | 15 | 45 | 12 | 1.5 |
| 125 | 70 | 55 | 60 | 15 | 45 | 12 | 1.0 |
| 125 | 70 | 55 | 60 | 15 | 45 | 12 | 1.2 |
| 125 | 70 | 55 | 60 | 15 | 45 | 12 | 1.5 |

Figure A.13 ― Cold formed fascia board

Table A.13 — Dimensions and properties of cold formed steel fascia board sections

| Nominal size mm | Dimension mm |  |  | Thickness mm | Mass kg/m |
| --- | --- | --- | --- | --- | --- |
|  | B | C | D or E | t | w |
| 150 x 30 | 150 | 30 | 13 | 1.0 | 1.80 |
| 150 x 30 | 150 | 30 | 13 | 1.2 | 2.17 |
| 150 x 30 | 150 | 30 | 13 | 1.5 | 2.58 |
| 190 x 30 | 190 | 30 | 13 | 1.2 | 2.38 |
| 190 x 30 | 190 | 30 | 13 | 1.5 | 2.88 |
| 200 x 30 | 200 | 30 | 13 | 1.2 | 2.67 |
| 200 x 30 | 200 | 30 | 13 | 1.5 | 3.25 |

Figure A.14 ― Omega sections

Table A.14 — Dimensions and properties of Omega sections

| Dimension mm |  |  |  | Thickness, t mm |
| --- | --- | --- | --- | --- |
| A | B | C | D |  |
| 35 | 50 | 45 | 17 | 1.0 |
| 35 | 50 | 45 | 17 | 1.2 |
| 35 | 50 | 45 | 17 | 1.5 |
| 35 | 50 | 45 | 17 | 2.0 |

Figure A.15 ― Cold formed inwardly lipped channel section

Table A.15 — Dimensions and properties for cold formed inwardly lipped channel sections

| Dimension mm |  |  | Thickness mm | Area cm2 | Mass per metre run kg/m | Centroid cm |  | Moment of inertia cm4 |  | Section modulus of elasticity cm3 |  | Radius of gyration cm |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| B | D | C | t | A | W | Cx | Cy | IXX | IYY | ZXX | ZYY | RXX | RYY |
| 50 | 75 | 20 | 1.5 | 3.1350 | 2.4610 | 2.0939 | 3.7500 | 29.0565 | 12.2259 | 7.7484 | 5.8388 | 3.0444 | 1.9748 |
| 50 | 75 | 20 | 2.0 | 4.1400 | 3.2499 | 2.0942 | 3.7500 | 37.8675 | 15.8185 | 10.0980 | 7.5535 | 3.0244 | 1.9547 |
| 50 | 100 | 20 | 2.0 | 4.6400 | 3.6424 | 1.8793 | 5.0000 | 73.9179 | 17.5943 | 14.7836 | 9.3621 | 3.9913 | 1.9473 |
| 50 | 100 | 20 | 2.5 | 5.7500 | 4.5138 | 1.8804 | 5.0000 | 90.6510 | 21.3501 | 18.1302 | 11.3538 | 3.9706 | 1.9269 |
| 50 | 125 | 20 | 2.0 | 5.1400 | 4.0349 | 1.7062 | 6.2500 | 124.4683 | 19.0249 | 19.9149 | 11.1503 | 4.9209 | 1.9239 |
| 50 | 125 | 20 | 2.5 | 6.3750 | 5.0044 | 1.7083 | 6.2500 | 153.0078 | 23.0905 | 24.4813 | 13.5164 | 4.8991 | 1.9032 |
| 50 | 138 | 20 | 2.0 | 5.4000 | 4.2390 | 1.6289 | 6.9000 | 157.0036 | 19.6643 | 22.7541 | 12.0722 | 5.3921 | 1.9083 |
| 50 | 138 | 20 | 2.5 | 6.7000 | 5.2595 | 1.6315 | 6.9000 | 193.1830 | 23.8674 | 27.9975 | 14.6289 | 5.3697 | 1.8874 |
| 50 | 150 | 20 | 2.0 | 5.6400 | 4.4274 | 1.5638 | 7.5000 | 191.0812 | 20.2022 | 25.4775 | 12.9184 | 5.8206 | 1.8926 |
| 50 | 150 | 20 | 2.5 | 7.0000 | 5.4950 | 1.5670 | 7.5000 | 235.2865 | 24.5207 | 31.3715 | 15.6485 | 5.7976 | 1.8716 |
| 50 | 150 | 20 | 3.0 | 8.3400 | 6.5469 | 1.5701 | 7.5000 | 278.1142 | 28.5692 | 37.0819 | 18.1953 | 5.7747 | 1.8508 |
| 50 | 163 | 20 | 2.0 | 5.9000 | 4.6315 | 1.4993 | 8.1500 | 232.5865 | 20.7357 | 28.5382 | 13.8300 | 6.2786 | 1.8747 |
| 50 | 163 | 20 | 2.5 | 7.3250 | 5.7501 | 1.5030 | 8.1500 | 286.5929 | 25.1682 | 35.1648 | 16.7454 | 6.2550 | 1.8536 |
| 50 | 163 | 20 | 3.0 | 8.7300 | 6.8531 | 1.5067 | 8.1500 | 338.9955 | 29.3235 | 41.5945 | 19.4621 | 6.2315 | 1.8327 |
| 50 | 175 | 20 | 2.0 | 6.1400 | 4.8199 | 1.4446 | 8.7500 | 275.3191 | 21.1880 | 31.4650 | 14.6668 | 6.6963 | 1.8576 |
| 50 | 175 | 20 | 2.5 | 7.6250 | 5.9856 | 1.4488 | 8.7500 | 339.4401 | 25.7170 | 38.7932 | 17.7509 | 6.6721 | 1.8365 |
| 50 | 175 | 20 | 3.0 | 9.0900 | 7.1357 | 1.4530 | 8.7500 | 401.7336 | 29.9626 | 45.9124 | 20.6216 | 6.6479 | 1.8155 |
| 63 | 175 | 20 | 2.0 | 6.6600 | 5.2281 | 1.9135 | 8.7500 | 314.2286 | 36.6786 | 35.9118 | 19.1682 | 6.8689 | 2.3468 |
| 63 | 175 | 20 | 2.5 | 8.2750 | 6.4959 | 1.9162 | 8.7500 | 387.7974 | 44.7463 | 44.3197 | 23.3511 | 6.8457 | 2.3254 |
| 63 | 175 | 20 | 3.0 | 9.8700 | 7.7480 | 1.9190 | 8.7500 | 459.4282 | 52.4013 | 52.5061 | 27.3066 | 6.8226 | 2.3042 |
| 50 | 200 | 20 | 2.0 | 6.6400 | 5.2124 | 1.3434 | 10.0000 | 378.7445 | 22.0256 | 37.8745 | 16.3958 | 7.5525 | 1.8213 |
| 50 | 200 | 20 | 2.5 | 8.2500 | 6.4763 | 1.3485 | 10.0000 | 467.4219 | 26.7325 | 46.7422 | 19.8241 | 7.5271 | 1.8001 |
| 50 | 200 | 20 | 3.0 | 9.8400 | 7.7244 | 1.3537 | 10.0000 | 553.7592 | 31.1445 | 55.3759 | 23.0076 | 7.5018 | 1.7791 |
| 75 | 200 | 20 | 2.0 | 7.6400 | 5.9974 | 2.2212 | 10.0000 | 476.7579 | 58.0380 | 47.6758 | 26.1291 | 7.8995 | 2.7562 |
| 75 | 200 | 20 | 2.5 | 9.5000 | 7.4575 | 2.2237 | 10.0000 | 589.3229 | 71.0351 | 58.9323 | 31.9448 | 7.8762 | 2.7345 |
| 75 | 200 | 20 | 3.0 | 11.3400 | 8.9019 | 2.2262 | 10.0000 | 699.3042 | 83.4600 | 69.9304 | 37.4901 | 7.8528 | 2.7129 |